# Type: Low-E Clear Reflective Insulating Glass

“Solarban®” R77 (2) Clear + Clear by Vitro Architectural Glass

Outdoor Lite: Clear (transparent) Float Glass by Vitro Architectural Glass, Sputter Coated on second surface (2)

Indoor Lite: Clear (transparent) Float Glass

Low-E Coating: “Solarban®” R77 Solar Control (Sputtered) by Vitro Architectural Glass

Location: Second Surface (2)

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 47% | 0.29 | 0.27 | 0.25 | 0.29 | 25% |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

# Outdoor Appearance: Clear

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Low-Iron Low-E Reflective Insulating Glass

“Solarban®” R77 (2) “Starphire®” + “Starphire®” by Vitro Architectural Glass

Outdoor Lite: “Starphire®” (low-iron [a specially formulated glass type to eliminate the green hue commonly associated with clear glass]) Float Glass by Vitro Architectural Glass, Sputter Coated on second surface (2)

Indoor Lite: “Starphire®” (low-iron) Float Glass

Low-E Coating: “Solarban®” R77 Solar Control (Sputtered) by Vitro Architectural Glass

Location: Second Surface (2)

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 50% | 0.29 | 0.27 | 0.25 | 0.29 | 26% |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Ultra-clear

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Low-Iron Low-E Reflective Insulating Glass

“Solarban®” R77 (2) “Acuity®” + “Acuity®” by Vitro Architectural Glass

Outdoor Lite: “Acuity®” (low-iron [a specially formulated glass type to eliminate the green hue commonly associated with clear glass]) Float Glass by Vitro Architectural Glass, Sputter Coated on second surface (2)

Indoor Lite: “Acuity®” (low-iron) Float Glass

Low-E Coating: “Solarban®” R77 Solar Control (Sputtered) by Vitro Architectural Glass

Location: Second Surface (2)

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 49% | 0.29 | 0.27 | 0.25 | 0.29 | 26% |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Ultra-clear

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Low-E Tinted Reflective Insulating Glass

“Solarban®” R77 (2) “Azuria®” + Clear by Vitro Architectural Glass

Outdoor Lite: “Azuria®” Glass by Vitro Architectural Glass, Sputter Coated on second surface (2)

Indoor Lite: Clear (transparent) Float Glass

Low-E Coating: “Solarban®” R77 Solar Control (Sputtered) by Vitro Architectural Glass

Location: Second Surface (2)

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 36% | 0.29 | 0.27 | 0.21 | 0.24 | 17% |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Aqua-blue

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Low-E Reflective Insulating Glass

“Solarban®” R77 (2) “Optiblue ®” + Clear by Vitro Architectural Glass

Outdoor Lite: “Optiblue®” Glass by Vitro Architectural Glass, Sputter Coated on second surface (2)

Indoor Lite: Clear (transparent) Float Glass

Low-E Coating: “Solarban®” R77 Solar Control (Sputtered) by Vitro Architectural Glass

Location: Second Surface (2)

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 34% | 0.29 | 0.27 | 0.21 | 0.24 | 15% |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Steel blue-gray

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Low-E Tinted Reflective Insulating Glass

“Solarban®” R77 (2) “Solargray®” + Clear by Vitro Architectural Glass

Outdoor Lite: “Solargray®” Glass by Vitro Architectural Glass, Sputter Coated on second surface (2)

Indoor Lite: Clear (transparent) Float Glass

Low-E Coating: “Solarban®” R77 Solar Control (Sputtered) by Vitro Architectural Glass

Location: Second Surface (2)

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 23% | 0.29 | 0.27 | 0.18 | 0.20 | 10% |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Cool light-gray

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Low-E Tinted Reflective Insulating Glass

“Solarban®” R77 (2) “Solexia ®” + Clear by Vitro Architectural Glass

Outdoor Lite: “Solexia®” Glass by Vitro Architectural Glass, Sputter Coated on second surface (2)

Indoor Lite: Clear (transparent) Float Glass

Low-E Coating: “Solarban®” R77 Solar Control (Sputtered) by Vitro Architectural Glass

Location: Second Surface (2)

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 41% | 0.29 | 0.27 | 0.23 | 0.26 | 20% |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Light-green

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Low-E Tinted Reflective Insulating Glass

“Solarban®” R77 (2) “Solarbronze ®” + Clear by Vitro Architectural Glass

Outdoor Lite: “Solarbronze®” Glass by Vitro Architectural Glass, Sputter Coated on second surface (2)

Indoor Lite: Clear (transparent) Float Glass

Low-E Coating: “Solarban®” R77 Solar Control (Sputtered) by Vitro Architectural Glass

Location: Second Surface (2)

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 28% | 0.29 | 0.27 | 0.19 | 0.22 | 12% |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Warm-bronze

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Low-E Tinted Reflective Insulating Glass

“Solarban®” R77 (2) “Solarblue ®” + Clear by Vitro Architectural Glass

Outdoor Lite: “Solarblue®” Glass by Vitro Architectural Glass, Sputter Coated on second surface (2)

Indoor Lite: Clear (transparent) Float Glass

Low-E Coating: “Solarban®” R77 Solar Control (Sputtered) by Vitro Architectural Glass

Location: Second Surface (2)

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 30% | 0.29 | 0.27 | 0.20 | 0.23 | 13% |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Light sky-blue

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Solar Control Tinted Insulating Glass

“Solarban®” R77 (2) “Optigray®” + Clear by Vitro Architectural Glass

Outdoor Lite: “Optigray®” Glass by Vitro Architectural Glass

Indoor Lite: Clear (transparent) Float Glass

Low-E Coating: “Solarban®” R77 Solar Control (Sputtered) by Vitro Architectural Glass

Location: Second Surface (2)

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 33% | 0.29 | 0.27 | 0.21 | 0.24 | 15% |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Ultra-neutral, light-gray

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass