# Type: Uncoated Tinted Insulating Glass

“Solarblue®” + Clear by Vitro Architectural Glass

Outdoor Lite: “Solarblue®” Float Glass Vitro Architectural Glass

Indoor Lite: Clear (transparent) Float Glass

Tint Color: “Solarblue®” by Vitro Architectural Glass

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 50% | 0.47 | 0.50 | 0.49 | 0.56 | 9% |

Approved Manufacturers: Vitro-specific approval not required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Light sky-blue

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Low-E Tinted Insulating Glass

“Solarblue®” + “Sungate®” 400 (3) Clear by Vitro Architectural Glass

Outdoor Lite: “Solarblue®” Glass by Vitro Architectural Glass

Indoor Lite: Clear (transparent) Float Glass Sputter Coated on third surface (3) Low-E Coating: “Sungate®” 400 (Sputtered) by Vitro Architectural Glass Location: Third Surface (3)

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 48% | 0.32 | 0.31 | 0.42 | 0.49 | 8% |

Approved Manufacturers: Vitro-specific approval not required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Light sky-blue

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Solar Control Low-E Tinted Insulating Glass

“Solarban®” 60 (2) “Solarblue®” + Clear by Vitro Architectural Glass

Outdoor Lite: “Solarblue®” Glass by Vitro Architectural Glass, Sputter Coated on second surface (2)

Indoor Lite: Clear (transparent) Float Glass

Low-E Coating: “Solarban®” 60 Solar Control (Sputtered) by Vitro Architectural Glass

Location: Second Surface (2)

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 45% | 0.29 | 0.27 | 0.28 | 0.33 | 7% |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Light sky-blue

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Solar Control Low-E Tinted Insulating Glass

“Solarblue®” + “Solarban®” 60 (3) Clear by Vitro Architectural Glass

Outdoor Lite: “Solarblue®” Glass by Vitro Architectural Glass

Indoor Lite: Clear (transparent) Float Glass, Sputter Coated on third surface (3)

Low-E Coating: “Solarban®” 60 Solar Control (Sputtered) by Vitro Architectural Glass

Location: Third Surface (3)

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 45% | 0.29 | 0.27 | 0.33 | 0.38 | 7% |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Light sky-blue

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Solar Control Low-E Tinted Insulating Glass

“Solarban®” 67 (2) “Solarblue®” + Clear by Vitro Architectural Glass

Outdoor Lite: “Solarblue®” Glass by Vitro Architectural Glass, Sputter Coated on second surface (2)

Indoor Lite: Clear (transparent) Float Glass

Low-E Coating: “Solarban®” 67 Solar Control (Sputtered) by Vitro Architectural Glass

Location: Second Surface (2)

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 34% | 0.29 | 0.27 | 0.23 | 0.26 | 10% |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Light sky-blue

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Solar Control Low-E Tinted Insulating Glass

“Solarblue®” + “Solarban®” 67 (3) Clear by Vitro Architectural Glass

Outdoor Lite: “Solarblue®” Glass by Vitro Architectural Glass

Indoor Lite: Clear (transparent) Float Glass, Sputter Coated on third surface (3)

Low-E Coating: “Solarban®” 67 Solar Control (Sputtered) by Vitro Architectural Glass

Location: Third Surface (3)

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 34% | 0.29 | 0.27 | 0.30 | 0.34 | 9% |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Light sky-blue

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Solar Control Low-E Clear Insulating Glass

“Solarban®” 70 (2) “Solarblue®” + Clear by Vitro Architectural Glass

Outdoor Lite: “Solarblue®” Glass by Vitro Architectural Glass, Sputter Coated on second surface (2)

Indoor Lite: Clear (transparent) Float Glass

Low-E Coating: “Solarban®” 70 Solar Control (Sputtered) by Vitro Architectural Glass

Location: Second Surface (2)

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 41% | 0.28 | 0.26 | 0.22 | 0.25 | 8% |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Light sky-blue

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Solar Control Low-E Tinted Insulating Glass

“Solarblue®” + “Solarban®” 70 (3) † by Vitro Architectural Glass

Outdoor Lite: “Solarblue®” Glass by Vitro Architectural Glass

Indoor Lite: Float Glass by Vitro Architectural Glass, Sputter Coated on third surface (3) †

Low-E Coating: “Solarban®” 70 Solar Control (Sputtered) by Vitro Architectural Glass

Location: Third Surface (3)

† Solarban® 70 for annealed applications is applied to Acuity™ glass; heat-treated applications will require either clear or Acuity™ glass depending on manufacturing process.

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 41% | 0.28 | 0.26 | 0.27 | 0.30 | 8% |

Approved Manufacturers: Vitro Certified™ Fabricator Required.

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Light sky-blue

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Reflective Low-E Tinted Reflective Insulating Glass

“Solarban®” R100 (2) “Solarblue®” + Clear by Vitro Architectural Glass

Outdoor Lite: “Solarblue®” Glass by Vitro Architectural Glass, Sputter Coated on second surface (2)

Indoor Lite: Clear (transparent) Float Glass

Low-E Coating: “Solarban®” R100 Solar Control (Sputtered) by Vitro Architectural Glass

Location: Second Surface (2)

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 26% | 0.29 | 0.27 | 0.19 | 0.22 | 15% |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Light sky-blue

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Solar Control Low-E Tinted Insulating Glass

“Solarban®” 90 (2) “Solarblue®” + Clear by Vitro Architectural Glass

Outdoor Lite: “Solarblue®” Glass by Vitro Architectural Glass, Sputter Coated on second surface (2)

Indoor Lite: Clear (transparent) Float Glass

Low-E Coating: “Solarban®” 90 Solar Control (Sputtered) by Vitro Architectural Glass

Location: Second Surface (2)

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 32% | 0.29 | 0.27 | 0.19 | 0.22 | 8% |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Light sky-blue

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Solar Control Low-E Tinted Insulating Glass

“Solarblue®” + “Solarban®” 90 (3) Clear by Vitro Architectural Glass

Outdoor Lite: “Solarblue®” Glass by Vitro Architectural Glass

Indoor Lite: Clear (transparent) Float Glass, Sputter Coated on third surface (3)

Low-E Coating: “Solarban®” 90 Solar Control (Sputtered) by Vitro Architectural Glass

Location: Third Surface (3)

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 32% | 0.29 | 0.27 | 0.25 | 0.29 | 10% |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Deep-blue

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Reflective Tinted Insulating Glass

“Solarcool®” (2) “Solarblue®” + Clear

Outdoor Lite: “Solarblue®” Glass by Vitro Architectural Glass

Indoor Lite: Clear (transparent) Float Glass

Reflective Coating: “Solarcool®” by Vitro Architectural Glass

Location: Second Surface (2)

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 20% | 0.47 | 0.50 | 0.32 | 0.37 | 15% |

Approved Manufacturers: Vitro-specific approval not required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Reflective light sky-blue

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Reflective Tinted Solar Control Low-E Insulating Glass

“Solarcool®” (2) “Solarblue®” + “Solarban®” 60 (3) Clear by Vitro Architectural Glass

Outdoor Lite: “Solarblue®” Glass by Vitro Architectural Glass

Indoor Lite: Clear (transparent) Float Glass, Sputter Coated on third surface (3)

Low-E Coating: “Solarban®” 60 Solar Control (Sputtered) by Vitro Architectural Glass

Location: Third Surface (3)

Reflective Coating: “Solarcool®” by Vitro Architectural Glass

Location: Second Surface (2)

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 17% | 0.29 | 0.27 | 0.18 | 0.21 | 14% |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Reflective light sky-blue

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Reflective Solar Control Low-E Insulating Glass

“Solarcool®” (2) “Solarblue®” + “Solarban®” 70 (3) † by Vitro Architectural Glass

Outdoor Lite: “Solarblue®” Glass by Vitro Architectural Glass

Indoor Lite: Float Glass by Vitro Architectural Glass, Sputter Coated on third surface (3) †

Low-E Coating: “Solarban®” 70 Solar Control (Sputtered) by Vitro Architectural Glass

Location: Third Surface (3)

Reflective Coating: “Solarcool®” by Vitro Architectural Glass

Location: Second Surface (2)

† Solarban® 70 for annealed applications is applied to Acuity™ glass; heat-treated applications will require either clear or Acuity™ glass depending on manufacturing process.

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 16% | 0.28 | 0.26 | 0.15 | 0.18 | 14% |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Reflective light sky-blue

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Reflective Tinted Solar Control Low-E Insulating Glass

“Solarcool®” (2) “Solarblue®” + “Solarban®” 90 (3) Clear by Vitro Architectural Glass

Outdoor Lite: “Solarblue®” Glass by Vitro Architectural Glass

Indoor Lite: Clear (transparent) Float Glass, Sputter Coated on third surface (3)

Low-E Coating: “Solarban®” 90 Solar Control (Sputtered) by Vitro Architectural Glass

Location: Third Surface (3)

Reflective Coating: “Solarcool®” by Vitro Architectural Glass

Location: Second Surface (2)

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 13% | 0.29 | 0.27 | 0.15 | 0.17 | 15% |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Reflective light sky-blue

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Reflective Tinted Insulating Glass

“Solarcool®” (1) “Solarblue®” + Clear

Outdoor Lite: “Solarblue®” Glass by Vitro Architectural Glass

Indoor Lite: Clear (transparent) Float Glass

Reflective Coating: “Solarcool®” by Vitro Architectural Glass

Location: First Surface (1)

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 19% | 0.47 | 0.50 | 0.29 | 0.33 | 37% |

Approved Manufacturers: Vitro-specific approval not required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Reflective light sky-blue

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Reflective Tinted Solar Control Low-E Insulating Glass

“Solarcool®” (1) “Solarblue®” + “Solarban®” 90 (3) Clear by Vitro Architectural Glass

Outdoor Lite: “Solarblue®” Glass by Vitro Architectural Glass

Indoor Lite: Clear (transparent) Float Glass, Sputter Coated on third surface (3)

Low-E Coating: “Solarban®” 90 Solar Control (Sputtered) by Vitro Architectural Glass

Location: Third Surface (3)

Reflective Coating: “Solarcool®” by Vitro Architectural Glass

Location: First Surface (1)

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 12% | 0.29 | 0.27 | 0.12 | 0.14 | 37% |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Reflective light sky-blue

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass