# Type: U-Value Enhancing Low-E Insulating Glass

“Solarban ®” 60 (2) Clear + “Sungate ThermL™”  (4) Clear by Vitro Architectural Glass.

Outdoor Lite: Clear (Transparent) Float Glass by Vitro Architectural Glass, Sputter Coated on second surface (2)

Indoor Lite: Clear (Transparent) Float Glass, Sputter Coated on third surface (3)

Low-E Coating: “Solarban®” 60 Solar Control (Sputtered) by Vitro Architectural Glass

Location: Second Surface (2)

U Value Enhancing Low-E Coating: “Sungate ThermL™”  by Vitro Architectural Glass

Location: Fourth Surface (4)

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 69% | 0.23 | 0.21 | 0.38 | 0.44 | 10% |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Clear

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: U-Value Enhancing Low-Iron Low-E Insulating Glass

“Solarban ®” 60 (2) “Starphire®” + “Sungate ThermL™”  (4) “Starphire®” by Vitro Architectural Glass.

Outdoor Lite: “Starphire®” (low-iron [a specially formulated glass type to eliminate the green hue commonly associated with clear glass]) Float Glass, Sputter Coated on second surface (2)

Indoor Lite: “Starphire®” (low-iron) Float Glass, Sputter Coated on third surface (3)

Low-E Coating: “Solarban®” 60 Solar Control (Sputtered) by Vitro Architectural Glass

Location: Second Surface (2)

U Value Enhancing Low-E Coating: “Sungate ThermL™”  by Vitro Architectural Glass

Location: Fourth Surface (4)

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 73% | 0.23 | 0.21 | 0.41 | 0.47 | 11% |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Ultra-clear

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: U-Value Enhancing Low-Iron Low-E Insulating Glass

“Solarban ®” 60 (2) “Acuity®” + “Sungate ThermL™”  (4) “Acuity®” by Vitro Architectural Glass.

Outdoor Lite: “Acuity®” (low-iron [a specially formulated glass type to eliminate the green hue commonly associated with clear glass]) Float Glass, Sputter Coated on second surface (2)

Indoor Lite: “Acuity®” (low-iron) Float Glass, Sputter Coated on third surface (3)

Low-E Coating: “Solarban®” 60 Solar Control (Sputtered) by Vitro Architectural Glass

Location: Second Surface (2)

U Value Enhancing Low-E Coating: “Sungate Therml™”  by Vitro Architectural Glass

Location: Fourth Surface (4)

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 71% | 0.23 | 0.21 | 0.40 | 0.46 | 11% |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Ultra-clear

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: U-Value Enhancing Low-E Insulating Glass

“Solarban ®” 70 (2) † + “Sungate ThermL™”  (4) Clear by Vitro Architectural Glass.

Outdoor Lite: Clear (Transparent) Float Glass by Vitro Architectural Glass, Sputter Coated on second surface (2) †

Indoor Lite: Clear (Transparent) Float Glass, Sputter Coated on third surface (3)

Low-E Coating: “Solarban®” 70 Solar Control (Sputtered) by Vitro Architectural Glass

Location: Second Surface (2)

U Value Enhancing Low-E Coating: “Sungate ThermL™”  by Vitro Architectural Glass

Location: Fourth Surface (4)

† Solarban® 70 for annealed applications is applied to Acuity® glass; heat-treated applications will require either clear or Acuity® glass depending on manufacturing process.

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 63% | 0.23 | 0.20 | 0.27 | 0.31 | 13% |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Clear

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: U-Value Enhancing Low-Iron Low-E Insulating Glass

“Solarban ®” 72 (2) “Starphire®” + “Sungate ThermL™”  (4) “Starphire®” by Vitro Architectural Glass.

Outdoor Lite: “Starphire®” (low-iron [a specially formulated glass type to eliminate the green hue commonly associated with clear glass]) Float Glass, Sputter Coated on second surface (2)

Indoor Lite: “Starphire®” (low-iron) Float Glass, Sputter Coated on third surface (3)

Low-E Coating: “Solarban®” 72 Solar Control (Sputtered) by Vitro Architectural Glass

Location: Second Surface (2)

U Value Enhancing Low-E Coating: “Sungate ThermL™”  by Vitro Architectural Glass

Location: Fourth Surface (4)

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 66% | 0.23 | 0.20 | 0.27 | 0.31 | 13% |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Ultra-clear

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: U-Value Enhancing Low-Iron Low-E Insulating Glass

“Solarban ®” 72 (2) “Acuity®” + “Sungate ThermL™”  (4) “Acuity®” by Vitro Architectural Glass.

Outdoor Lite: “Acuity®” (low-iron [a specially formulated glass type to eliminate the green hue commonly associated with clear glass]) Float Glass, Sputter Coated on second surface (2)

Indoor Lite: “Acuity®” (low-iron) Float Glass, Sputter Coated on third surface (3)

Low-E Coating: “Solarban®” 72 Solar Control (Sputtered) by Vitro Architectural Glass

Location: Second Surface (2)

U Value Enhancing Low-E Coating: “Sungate ThermL™”  by Vitro Architectural Glass

Location: Fourth Surface (4)

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 65% | 0.23 | 0.20 | 0.27 | 0.31 | 13% |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Ultra-clear

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: U-Value Enhancing Low-E Insulating Glass

“Solarban ®” 90 (2) Clear + “Sungate ThermL™”  (4) Clear by Vitro Architectural Glass.

Outdoor Lite: Clear (Transparent) Float Glass by Vitro Architectural Glass, Sputter Coated on second surface (2)

Indoor Lite: Clear (Transparent) Float Glass, Sputter Coated on third surface (3)

Low-E Coating: “Solarban®” 90 Solar Control (Sputtered) by Vitro Architectural Glass

Location: Second Surface (2)

U Value Enhancing Low-E Coating: “Sungate ThermL™”  by Vitro Architectural Glass

Location: Fourth Surface (4)

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 50% | 0.23 | 0.21 | 0.23 | 0.26 | 12% |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Clear

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: U-Value Enhancing Low-Iron Low-E Insulating Glass

“Solarban ®” 90 (2) “Starphire®” + “Sungate ThermL™”  (4) “Starphire®” by Vitro Architectural Glass.

Outdoor Lite: “Starphire®” (low-iron [a specially formulated glass type to eliminate the green hue commonly associated with clear glass]) Float Glass, Sputter Coated on second surface (2)

Indoor Lite: “Starphire®” (low-iron) Float Glass, Sputter Coated on third surface (3)

Low-E Coating: “Solarban®” 90 Solar Control (Sputtered) by Vitro Architectural Glass

Location: Second Surface (2)

U Value Enhancing Low-E Coating: “Sungate ThermL™”  by Vitro Architectural Glass

Location: Fourth Surface (4)

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 52% | 0.23 | 0.21 | 0.22 | 0.26 | 12% |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Ultra-clear

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: U-Value Enhancing Low-Iron Low-E Insulating Glass

“Solarban ®” 90 (2) “Acuity®” + “Sungate ThermL™”  (4) “Acuity®” by Vitro Architectural Glass.

Outdoor Lite: “Acuity®” (low-iron [a specially formulated glass type to eliminate the green hue commonly associated with clear glass]) Float Glass, Sputter Coated on second surface (2)

Indoor Lite: “Acuity®” (low-iron) Float Glass, Sputter Coated on third surface (3)

Low-E Coating: “Solarban®” 90 Solar Control (Sputtered) by Vitro Architectural Glass

Location: Second Surface (2)

U Value Enhancing Low-E Coating: “Sungate ThermL™”  by Vitro Architectural Glass

Location: Fourth Surface (4)

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 52% | 0.23 | 0.21 | 0.23 | 0.26 | 12% |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Ultra-clear

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass