Type: Uncoated Tinted Insulating Glass “Graylite®” II + Clear by Vitro Architectural Glass

Outdoor Lite: “Graylite®” II Glass by Vitro Architectural Glass

Indoor Lite: Clear (transparent) Float Glass

Tint Color: “Graylite®” II by Vitro Architectural Glass

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 8% | 0.47 | 0.50 | 0.22 | 0.25 | 4% |

Approved Manufacturers: Vitro-specific approval not required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Dark-gray

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Solar Control Low-E Tinted Insulating Glass

“Graylite®” II + “Solarban®” 60 (3) Clear by Vitro Architectural Glass

Outdoor Lite: “Graylite®” II Glass by Vitro Architectural Glass

Indoor Lite: Clear (transparent) Float Glass, Sputter Coated on third surface (3)

Low-E Coating: “Solarban®” 60 Solar Control (Sputtered) by Vitro Architectural Glass

Location: Third Surface (3)

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 7% | 0.29 | 0.27 | 0.13 | 0.15 | 4% |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Dark-gray

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Solar Control Low-E Tinted Insulating Glass

“Graylite®” II + “Solarban®” 67 (3) Clear by Vitro Architectural Glass

Outdoor Lite: “Graylite®” II Glass by Vitro Architectural Glass

Indoor Lite: Clear (transparent) Float Glass, Sputter Coated on third surface (3)

Low-E Coating: “Solarban®” 67 Solar Control (Sputtered) by Vitro Architectural Glass

Location: Third Surface (3)

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 5% | 0.29 | 0.27 | 0.12 | 0.14 | 4% |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Dark-gray

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Solar Control Low-E Tinted Insulating Glass

“Graylite®” II + “Solarban®” 70 (3) † by Vitro Architectural Glass

Outdoor Lite: “Graylite®” II Glass by Vitro Architectural Glass

Indoor Lite: Float Glass by Vitro Architectural Glass, Sputter Coated on third surface (3) †

Low-E Coating: “Solarban®” 70 Solar Control (Sputtered) by Vitro Architectural Glass

Location: Third Surface (3)

† Solarban® 70 for annealed applications is applied to Acuity™ glass; heat-treated applications will require either clear or Acuity™ glass depending on manufacturing process.

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 6% | 0.28 | 0.26 | 0.11 | 0.13 | 4% |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Dark-gray

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Solar Control Low-E Tinted Insulating Glass

“Graylite®” II + “Solarban®” 90 (3) Clear by Vitro Architectural Glass

Outdoor Lite: “Graylite®” II Glass by Vitro Architectural Glass

Indoor Lite: Clear (transparent) Float Glass, Sputter Coated on third surface (3)

Low-E Coating: “Solarban®” 90 Solar Control (Sputtered) by Vitro Architectural Glass

Location: Third Surface (3)

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 5% | 0.29 | 0.27 | 0.11 | 0.13 | 4% |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Dark-gray

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Reflective Tinted Low-E Insulating Glass

“Graylite®” II + “Sungate®” 400 (3) Clear by Vitro Architectural Glass

Outdoor Lite: “Graylite®” II Glass by Vitro Architectural Glass

Indoor Lite: Clear (transparent) Float Glass Sputter Coated on third surface (3) Low-E Coating: “Sungate®” 400 (Sputtered) by Vitro Architectural Glass Location: Third Surface (3)

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 8% | 0.32 | 0.31 | 0.15 | 0.17 | 4% |

Approved Manufacturers: Vitro-specific approval not required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Dark-gray

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass