# Type: Solar Control Low-E Clear Insulating Glass

“Solarban®” 70 (2)† + Clear by Vitro Architectural Glass

Outdoor Lite: † Float Glass by Vitro Architectural Glass, Sputter Coated on second surface (2)

Indoor Lite: Clear (transparent) Float Glass

Low-E Coating: “Solarban®” 70 Solar Control (Sputtered) by Vitro Architectural Glass

Location: Second Surface (2)

†Solarban® 70 for annealed applications is applied to Acuity™ glass; heat-treated applications will either require clear or Acuity™ glass depending on manufacturing process.

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 64% | 0.28 | 0.26 | 0.27 | 0.32 | 13% |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

# Outdoor Appearance: Clear

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Solar Control Low-E Clear Insulating Glass

“Solarban®” 70 (2) “Azuria®” + Clear by Vitro Architectural Glass.

Outdoor Lite: “Azuria®” Glass by Vitro Architectural Glass, Sputter Coated on second surface (2)

Indoor Lite: Clear (transparent) Float Glass

Low-E Coating: “Solarban®” 70 Solar Control (Sputtered) by Vitro Architectural Glass

Location: Second Surface (2)

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 50% | 0.28 | 0.26 | 0.24 | 0.27 | 10% |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Aqua-blue, low-reflective glass

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Solar Control Low-E Clear Insulating Glass

“Solarban®” 70 (2) “Solargray®” + Clear by Vitro Architectural Glass

Outdoor Lite: “Solargray®” Glass by Vitro Architectural Glass, Sputter Coated on second surface (2)

Indoor Lite: Clear (transparent) Float Glass

Low-E Coating: “Solarban®” 70 Solar Control (Sputtered) by Vitro Architectural Glass

Location: Second Surface (2)

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 32% | 0.28 | 0.26 | 0.19 | 0.24 | 7% |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

# Outdoor Appearance: Gray

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Solar Control Low-E Clear Insulating Glass

“Solarban®” 70 (2) “Solexia ®” + Clear by Vitro Architectural Glass

Outdoor Lite: “Solexia®” Glass by Vitro Architectural Glass, Sputter Coated on second surface (2)

Indoor Lite: Clear (transparent) Float Glass

Low-E Coating: “Solarban®” 70 Solar Control (Sputtered) by Vitro Architectural Glass

Location: Second Surface (2)

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 56% | 0.28 | 0.26 | 0.26 | 0.29 | 11% |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Light-green, low-reflective glass

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Solar Control Low-E Clear Insulating Glass

“Solarban®” 70 (2) “Solarbronze ®” + Clear by Vitro Architectural Glass

Outdoor Lite: “Solarbronze®” Glass by Vitro Architectural Glass, Sputter Coated on second surface (2)

Indoor Lite: Clear (transparent) Float Glass

Low-E Coating: “Solarban®” 70 Solar Control (Sputtered) by Vitro Architectural Glass

Location: Second Surface (2)

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 39% | 0.28 | 0.26 | 0.20 | 0.23 | 8% |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Warm-bronze

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Solar Control Low-E Clear Insulating Glass

“Solarban®” 70 (2) “Solarblue ®” + Clear by Vitro Architectural Glass

Outdoor Lite: “Solarblue®” Glass by Vitro Architectural Glass, Sputter Coated on second surface (2)

Indoor Lite: Clear (transparent) Float Glass

Low-E Coating: “Solarban®” 70 Solar Control (Sputtered) by Vitro Architectural Glass

Location: Second Surface (2)

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 42% | 0.28 | 0.26 | 0.23 | 0.26 | 8% |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Light sky-blue

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Solar Control Tinted Insulating Glass

“Solarban®” 70 (2) “Optigray®” + Clear by Vitro Architectural Glass

Outdoor Lite: “Optigray®” Glass by Vitro Architectural Glass

Indoor Lite: Clear (transparent) Float Glass

Low-E Coating: “Solarban®” 70 Solar Control (Sputtered) by Vitro Architectural Glass

Location: Second Surface (2)

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 46% | 0.28 | 0.26 | 0.23 | 0.26 | 9% |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Ultra-neutral, light-gray, low-e glass

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Solar Control Low-E Insulating Glass

“Solarban®” 70 (2) “Optiblue®” + Clear (Formerly Solarban® z75) by Vitro Architectural Glass

Outdoor Lite: “Solarban® 70 (2) Optiblue®” Glass by Vitro Architectural Glass, Sputter Coated on second surface (2)

Indoor Lite: Clear (transparent) Float Glass

Low-E Coating: “Solarban®” 70 Solar Control (Sputtered) by Vitro Architectural Glass

Location: Second Surface (2)

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 46% | 0.28 | 0.26 | 0.23 | 0.26 | 9% |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Steel blue-gray

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Solar Control Low-E Tinted Insulating Glass

“Solexia®” + “Solarban®” 70 (3) † by Vitro Architectural Glass

Outdoor Lite: “Solexia®” Glass by Vitro Architectural Glass

Indoor Lite: Float Glass by Vitro Architectural Glass, Sputter Coated on third surface (3)†

Low-E Coating: “Solarban®” 70 Solar Control (Sputtered) by Vitro Architectural Glass

Location: Third Surface (3)

†Solarban® 70 for annealed applications is applied to Acuity™ glass; heat-treated applications will require either clear or Acuity™ glass depending on manufacturing process.

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 56% | 0.28 | 0.26 | 0.32 | 0.37 | 11% |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Emerald-green

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

Type: Solar Control Low-E Tinted Insulating Glass

“Atlantica®” + “Solarban®” 70 (3) † by Vitro Architectural Glass

Outdoor Lite: “Atlantica®” Glass by Vitro Architectural Glass

Indoor Lite: Float Glass by Vitro Architectural Glass, Sputter Coated on third surface (3)†

Low-E Coating: “Solarban®” 70 Solar Control (Sputtered) by Vitro Architectural Glass

Location: Third Surface (3)

† Solarban® 70 for annealed applications is applied to Acuity® glass; heat-treated applications will require either clear or Acuity® glass depending on manufacturing process.

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 49% | 0.28 | 0.26 | 0.29 | 0.33 | 9% |

Approved Manufacturers: Vitro Certified™ Fabricator Required.

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Emerald-green

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Solar Control Low-E Tinted Insulating Glass

“Azuria®” + “Solarban®” 70 (3) † by Vitro Architectural Glass

Outdoor Lite: “Azuria®” Glass by Vitro Architectural Glass

Indoor Lite: Float Glass by Vitro Architectural Glass, Sputter Coated on third surface (3) †

Low-E Coating: “Solarban®” 70 Solar Control (Sputtered) by Vitro Architectural Glass

Location: Third Surface (3)

† Solarban® 70 for annealed applications is applied to Acuity® glass; heat-treated applications will require either clear or Acuity® glass depending on manufacturing process.

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 49% | 0.28 | 0.26 | 0.29 | 0.33 | 9% |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Aqua-blue

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Solar Control Low-E Tinted Insulating Glass

“Solarbronze®” + “Solarban®” 70 (3) † by Vitro Architectural Glass

Outdoor Lite: ”Solarbronze®” Glass by Vitro Architectural Glass

Indoor Lite: Float Glass by Vitro Architectural Glass, Sputter Coated on third surface (3) †

Low-E Coating: “Solarban®” 70 (Sputtered) by Vitro Architectural Glass

Location: Third Surface (3)

† Solarban® 70 for annealed applications is applied to Acuity® glass; heat-treated applications will require either clear or Acuity® glass depending on manufacturing process.

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 38% | 0.28 | 0.26 | 0.26 | 0.30 | 8% |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Warm-bronze

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Solar Control Low-E Tinted Insulating Glass

“Solargray®” + “Solarban®” 70 (3) † by Vitro Architectural Glass

Outdoor Lite: “Solargray®” Glass by Vitro Architectural Glass

Indoor Lite: Float Glass by Vitro Architectural Glass, Sputter Coated on third surface (3) †

Low-E Coating: “Solarban®” 70 (Sputtered) by Vitro Architectural Glass

Location: Third Surface

† Solarban® 70 for annealed applications is applied to Acuity® glass; heat-treated applications will require either clear or Acuity® glass depending on manufacturing process.

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 32% | 0.28 | 0.26 | 0.24 | 0.27 | 7% |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

# Outdoor Appearance: Gray

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Solar Control Low-E Tinted Insulating Glass

“Graylite®” II + “Solarban®” 70 (3) † by Vitro Architectural Glass

Outdoor Lite: “Graylite®” II Glass by Vitro Architectural Glass

Indoor Lite: Float Glass by Vitro Architectural Glass, Sputter Coated on third surface (3) †

Low-E Coating: “Solarban®” 70 Solar Control (Sputtered) by Vitro Architectural Glass

Location: Third Surface (3)

† Solarban® 70 for annealed applications is applied to Acuity® glass; heat-treated applications will require either clear or Acuity® glass depending on manufacturing process.

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 6% | 0.28 | 0.26 | 0.11 | 0.13 | 4% |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Dark-gray

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Solar Control Low-E Tinted Insulating Glass

“Solarblue®” + “Solarban®” 70 (3) † by Vitro Architectural Glass

Outdoor Lite: “Solarblue®” Glass by Vitro Architectural Glass

Indoor Lite: Float Glass by Vitro Architectural Glass, Sputter Coated on third surface (3) †

Low-E Coating: “Solarban®” 70 Solar Control (Sputtered) by Vitro Architectural Glass

Location: Third Surface (3)

†Solarban® 70 for annealed applications is applied to Acuity® glass; heat-treated applications will require either clear or Acuity® glass depending on manufacturing process.

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 41% | 0.28 | 0.26 | 0.27 | 0.30 | 8% |

Approved Manufacturers: Vitro Certified™ Fabricator Required.

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Sky-blue

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Solar Control Low-E Tinted Insulating Glass

“Pacifica®” + “Solarban®” 70 (3) † by Vitro Architectural Glass

Outdoor Lite: “Pacifica®” Glass by Vitro Architectural Glass

Indoor Lite: Float Glass by Vitro Architectural Glass, Sputter Coated on third surface (3) †

Low-E Coating: “Solarban®” 70 Solar Control (Sputtered) by Vitro Architectural Glass

Location: Third Surface (3)

† Solarban® 70 for annealed applications is applied to Acuity® glass; heat-treated applications will require either clear or Acuity® glass depending on manufacturing process.

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 31% | 0.28 | 0.26 | 0.22 | 0.26 | 6% |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Deep-blue

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Solar Control Tinted Insulating Glass

“Optigray®” + “Solarban®” 70 (3) † by Vitro Architectural Glass

Outdoor Lite: “Optigray®” Glass by Vitro Architectural Glass

Indoor Lite: Float Glass by Vitro Architectural Glass, Sputter Coated on third surface (3) †

Low-E Coating: “Solarban®” 70 Solar Control (Sputtered) by Vitro Architectural Glass

Location: Third Surface (3)

†Solarban® 70 for annealed applications is applied to Acuity® glass; heat-treated applications will require either clear or Acuity® glass depending on manufacturing process.

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 46% | 0.28 | 0.26 | 0.28 | 0.32 | 9% |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Ultra-neutral, light-gray, low-e glass

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Subtly Reflective Solar Control Low-E Insulating Glass

“Vistacool®” (2) “Azuria®” + “Solarban®” 70 (3) † by Vitro Architectural Glass

Outdoor Lite: “Azuria®” Glass by Vitro Architectural Glass

Indoor Lite: Float Glass by Vitro Architectural Glass, Sputter Coated on third surface (3) †

Low-E Coating: “Solarban®” 70 Solar Control (Sputtered) by Vitro Architectural Glass

Location: Third Surface (3)

Reflective Coating: “Vistacool®” by Vitro Architectural Glass

Location: Second Surface (2)

† Solarban® 70 for annealed applications is applied to Acuity® glass; heat-treated applications will require either clear or Acuity® glass depending on manufacturing process.

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 38% | 0.28 | 0.26 | 0.24 | 0.28 | 21% |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Subtly reflective aqua-blue

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Subtly Reflective Solar Control Low-E Insulating Glass

“Vistacool®” (2) “Pacifica®” + “Solarban®” 70 (3) † by Vitro Architectural Glass

Outdoor Lite: “Pacifica®” Glass by Vitro Architectural Glass

Indoor Lite: Float Glass by Vitro Architectural Glass, Sputter Coated on third surface (3) †

Low-E Coating: “Solarban®” 70 Solar Control (Sputtered) by Vitro Architectural Glass

Location: Third Surface (3)

Reflective Coating: “Vistacool®” by Vitro Architectural Glass

Location: Second Surface (2)

† Solarban® 70 for annealed applications is applied to Acuity® glass; heat-treated applications will require either clear or Acuity® glass depending on manufacturing process..

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 24% | 0.28 | 0.26 | 0.19 | 0.22 | 11% |

Approved Manufacturers: Vitro Recommended Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Subtly reflective deep-blue

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Reflective Solar Control Low-E Insulating Glass

“Solarcool®” (2) “Azuria®” + “Solarban®” 70 (3) † by Vitro Architectural Glass

Outdoor Lite: “Azuria®” Glass by Vitro Architectural Glass

Indoor Lite: Float Glass by Vitro Architectural Glass, Sputter Coated on third surface (3) †

Low-E Coating: “Solarban®” 70 Solar Control (Sputtered) by Vitro Architectural Glass

Location: Third Surface (3)

Reflective Coating: “Solarcool®” by Vitro Architectural Glass

Location: Second Surface (2)

† Solarban® 70 for annealed applications is applied to Acuity® glass; heat-treated applications will require either clear or Acuity® glass depending on manufacturing process.

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 19% | 0.28 | 0.26 | 0.16 | 0.18 | 19% |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Aqua-blue

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Reflective Solar Control Low-E Insulating Glass

“Solarcool®” (2) “Solarbronze ®” + “Solarban®” 70 (3) † by Vitro Architectural Glass

Outdoor Lite: “Solarbronze®” Glass by Vitro Architectural Glass

Indoor Lite: Float Glass by Vitro Architectural Glass, Sputter Coated on third surface (3) †

Low-E Coating: “Solarban®” 70 Solar Control (Sputtered) by Vitro Architectural Glass

Location: Third Surface (3)

Reflective Coating: “Solarcool®” by Vitro Architectural Glass

Location: Second Surface (2)

† Solarban® 70 for annealed applications is applied to Acuity® glass; heat-treated applications will require either clear or Acuity® glass depending on manufacturing process.

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 15% | 0.28 | 0.26 | 0.15 | 0.17 | 14% |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Bronze-metallic

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Reflective Solar Control Low-E Insulating Glass

“Solarcool ®” (2) “Solargray®” + “Solarban®” 70 (3) † by Vitro Architectural Glass

Outdoor Lite: “Solargray®” Glass by Vitro Architectural Glass

Indoor Lite: Float glass by Vitro Architectural Glass, Sputter Coated on third surface (3) †

Low-E Coating: “Solarban®” 70 Solar Control (Sputtered) by Vitro Architectural Glass

Location: Third Surface (3)

Reflective Coating: “Solarcool®” by Vitro Architectural Glass

Location: Second Surface (2)

† Solarban® 70 for annealed applications is applied to Acuity® glass; heat-treated applications will require either clear or Acuity® glass depending on manufacturing process.

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 13% | 0.28 | 0.26 | 0.14 | 0.16 | 11% |

Approved Manufacturers: Vitro Certified™ Fabricator required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Gray-metallic

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Reflective Solar Control Low-E Insulating Glass

“Solarcool ®” (2) “Solarblue ®” + “Solarban®” 70 (3) † by Vitro Architectural Glass

Outdoor Lite: “Solarblue®” Glass by Vitro Architectural Glass

Indoor Lite: Float glass by Vitro Architectural Glass, Sputter Coated on third surface (3) †

Low-E Coating: “Solarban®” 70 Solar Control (Sputtered) by Vitro Architectural Glass

Location: Third Surface (3)

Reflective Coating: “Solarcool®” by Vitro Architectural Glass

Location: Second Surface (2)

† Solarban® 70 for annealed applications is applied to Acuity® glass; heat-treated applications will require either clear or Acuity® glass depending on manufacturing process.

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 16% | 0.28 | 0.26 | 0.15 | 0.18 | 14% |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Sky-blue metallic

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Reflective Solar Control Low-E Insulating Glass

“Solarcool®” (2) “Pacifica®” + “Solarban®” 70 (3) † by Vitro Architectural Glass

Outdoor Lite: “Pacifica®” Glass by Vitro Architectural Glass

Indoor Lite: Float Glass by Vitro Architectural Glass, Sputter Coated on third surface (3) †

Low-E Coating: “Solarban®” 70 Solar Control (Sputtered) by Vitro Architectural Glass

Location: Third Surface (3)

Reflective Coating: “Solarcool®” by Vitro Architectural Glass

Location: Second Surface (2)

† Solarban® 70 for annealed applications is applied to Acuity® glass; heat-treated applications will require either clear or Acuity® glass depending on manufacturing process.

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 12% | 0.28 | 0.26 | 0.13 | 0.15 | 10% |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Deep-blue

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass