# Type: Solar Control Low-E Clear Insulating Glass

***“Solarban*®*”* 60 (2) Clear + Clear** by Vitro Architectural Glass

**Outdoor Lite:** Clear Glass, Sputter Coated on second surface (2)

**Indoor Lite:** Clear (transparent) Float Glass

**Low-E Coating: *“Solarban®”*** 60 Solar Control (Sputtered) by Vitro Architectural Glass

**Location:** Second Surface (2)

# Performance Values

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| 70% | 0.29 | 0.27 | 0.39 | 0.45 | 11% |

**Approved Manufacturers:** Vitro Certified™ Fabricator Required

**Certification:** Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation [Institute (www.c2ccertified.org](http://www.c2ccertified.org/)).

# Outdoor Appearance: Clear

**Insulating Unit Construction:** 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Solar Control Low-Iron Low-E Clear Insulating Glass

***“Solarban*®*”* 60 (2) “*Starphire*®*”* + *“Starphire®”*** by Vitro Architectural Glass

**Outdoor Lite: *“Starphire”*** (low-iron [a specially formulated glass type to eliminate the green hue commonly associated with clear glass]) Float Glass by Vitro Architectural Glass, Sputter Coated on second surface (2)

**Indoor Lite: *“Starphire®”*** (low-iron) Float Glass

**Low-E Coating: *“Solarban®”*** 60 Solar Control (Sputtered) by Vitro Architectural Glass

**Location:** Second Surface (2)

# Performance Values

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| 74% | 0.29 | 0.27 | 0.41 | 0.48 | 11% |

**Approved Manufacturers:** Vitro Certified™ Fabricator Required

**Certification:** Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation [Institute (www.c2ccertified.org](http://www.c2ccertified.org/)).

**Outdoor Appearance:** Ultra-clear

**Insulating Unit Construction:** 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Solar Control Low-Iron Low-E Clear Insulating Glass

***“Solarban*®*”* 60 (2) “*Acuity™”* + *“Acuity™”*** by Vitro Architectural Glass

**Outdoor Lite: *“Acuity™”*** (low-iron [a specially formulated glass type to eliminate the green hue commonly associated with clear glass]) Float Glass by Vitro Architectural Glass, Sputter Coated on second surface (2)

**Indoor Lite: *“Acuity™”*** (low-iron) Float Glass

**Low-E Coating: *“Solarban®”*** 60 Solar Control (Sputtered) by Vitro Architectural Glass

**Location:** Second Surface (2)

# Performance Values

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| 73% | 0.29 | 0.27 | 0.41 | 0.47 | 11% |

**Approved Manufacturers:** Vitro Certified™ Fabricator Required

**Certification:** Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation [Institute (www.c2ccertified.org](http://www.c2ccertified.org/)).

**Outdoor Appearance:** Ultra-clear

**Insulating Unit Construction:** 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Solar Control Low-E Tinted Insulating Glass

***“Solarban*®*”* 60 (2) *“Atlantica*®*”* + Clear** by Vitro Architectural Glass

**Outdoor Lite: *“Atlantica®”*** Glass by Vitro Architectural Glass, Sputter Coated on second surface (2)

**Indoor Lite:** Clear (transparent) Float Glass

**Low-E Coating: *“Solarban®”*** 60 Solar Control (Sputtered) by Vitro Architectural Glass

**Location:** Second Surface (2)

# Performance Values

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| 53% | 0.29 | 0.27 | 0.27 | 0.32 | 8% |

**Approved Manufacturers:** Vitro Certified™ Fabricator Required

**Certification:** Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation [Institute (www.c2ccertified.org](http://www.c2ccertified.org/)).

**Outdoor Appearance:** Emerald-green

**Insulating Unit Construction:** 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Solar Control Low-E Tinted Insulating Glass

***“Solarban*®*”* 60 (2) *“Azuria*®*”* + Clear** by Vitro Architectural Glass

**Outdoor Lite: *“Azuria®”*** Glass by Vitro Architectural Glass, Sputter Coated on second surface (2)

**Indoor Lite:** Clear (transparent) Float Glass

**Low-E Coating: *“Solarban®”*** 60 Solar Control (Sputtered) by Vitro Architectural Glass

**Location:** Second Surface (2)

# Performance Values

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| 54% | 0.29 | 0.27 | 0.28 | 0.32 | 8% |

**Approved Manufacturers:** Vitro Certified™ Fabricator Required

**Certification:** Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation [Institute (www.c2ccertified.org](http://www.c2ccertified.org/)).

**Outdoor Appearance:** Aqua-blue

**Insulating Unit Construction:** 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Solar Control Low-E Tinted Insulating Glass

***“Solarban*®*”* 60 (2) *“Solargray*®*”* + Clear** by Vitro Architectural Glass

**Outdoor Lite: *“Solargray®”*** Glass by Vitro Architectural Glass, Sputter Coated on second surface (2)

**Indoor Lite:** Clear (transparent) Float Glass

**Low-E Coating: *“Solarban®”*** 60 Solar Control (Sputtered) by Vitro Architectural Glass

**Location:** Second Surface (2)

# Performance Values

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| 35% | 0.29 | 0.27 | 0.25 | 0.29 | 6% |

**Approved Manufacturers:** Vitro Certified™ Fabricator Required

**Certification:** Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation [Institute (www.c2ccertified.org](http://www.c2ccertified.org/)).

**Outdoor Appearance:** Cool light-gray

**Insulating Unit Construction:** 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Solar Control Low-E Tinted Insulating Glass

***“Solarban*®*”* 60 (2) *“Solexia*®*”* + Clear** by Vitro Architectural Glass

**Outdoor Lite: *“Solexia®”*** Glass by Vitro Architectural Glass, Sputter Coated on second surface (2)

**Indoor Lite:** Clear (transparent) Float Glass

**Low-E Coating: *“Solarban®”*** 60 Solar Control (Sputtered) by Vitro Architectural Glass

**Location:**

Second Surface (2)

# Performance Values

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| 61% | 0.29 | 0.27 | 0.32 | 0.37 | 9% |

**Approved Manufacturers:** Vitro Certified™ Fabricator Required

**Certification:** Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation [Institute (www.c2ccertified.org](http://www.c2ccertified.org/)).

**Outdoor Appearance:** Light-green

**Insulating Unit Construction:** 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Solar Control Low-E Tinted Insulating Glass

***“Solarban*®*”* 60 (2) *“Solarbronze*®*”* + Clear** by Vitro Architectural Glass

**Outdoor Lite: *“Solarbronze®”*** Glass by Vitro Architectural Glass, Sputter Coated on second surface (2)

**Indoor Lite:** Clear (transparent) Float Glass

**Low-E Coating: *“Solarban®”*** 60 Solar Control (Sputtered) by Vitro Architectural Glass

**Location:** Second Surface (2)

# Performance Values

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| 42% | 0.29 | 0.27 | 0.28 | 0.32 | 7% |

**Approved Manufacturers:** Vitro Certified™ Fabricator Required

**Certification:** Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation [Institute (www.c2ccertified.org](http://www.c2ccertified.org/)).

**Outdoor Appearance:** Warm-bronze

**Insulating Unit Construction:** 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Solar Control Low-E Tinted Insulating Glass

***“Solarban*®*”* 60 (2) *“Solarblue*®*”* + Clear** by Vitro Architectural Glass

**Outdoor Lite: *“Solarblue®”*** Glass by Vitro Architectural Glass, Sputter Coated on second surface (2)

**Indoor Lite:** Clear (transparent) Float Glass

**Low-E Coating: *“Solarban®”*** 60 Solar Control (Sputtered) by Vitro Architectural Glass

**Location:** Second Surface (2)

# Performance Values

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| 45% | 0.29 | 0.27 | 0.29 | 0.33 | 7% |

**Approved Manufacturers:** Vitro Certified™ Fabricator Required

**Certification:** Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation [Institute (www.c2ccertified.org](http://www.c2ccertified.org/)).

**Outdoor Appearance:** Light sky-blue

**Insulating Unit Construction:** 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Solar Control Low-E Tinted Insulating Glass

***“Solarban*®*”* 60 (2) *“Pacifica*®*”* + Clear** by Vitro Architectural Glass

**Outdoor Lite: *“Pacifica®”*** Glass by Vitro Architectural Glass, Sputter Coated on second surface (2)

**Indoor Lite:** Clear (transparent) Float Glass

**Low-E Coating: *“Solarban®”*** 60 Solar Control (Sputtered) by Vitro Architectural Glass

**Location:** Second Surface (2)

# Performance Values

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| 34% | 0.29 | 0.27 | 0.23 | 0.26 | 6% |

**Approved Manufacturers:** Vitro Certified™ Fabricator Required

**Certification:** Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation [Institute (www.c2ccertified.org](http://www.c2ccertified.org/)).

**Outdoor Appearance:** Deep-blue

**Insulating Unit Construction:** 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Solar Control Tinted Insulating Glass

**“*Solarban*®” 60 (2) “*Optigray*®*”* + Clear** by Vitro Architectural Glass

**Outdoor Lite: “*Optigray®”*** Glass by Vitro Architectural Glass

**Indoor Lite:** Clear (transparent) Float Glass

**Low-E Coating: *“Solarban®”*** 60 Solar Control (Sputtered) by Vitro Architectural Glass

**Location:** Second Surface (2)

# Performance Values

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| 50% | 0.29 | 0.27 | 0.30 | 0.35 | 8% |

**Approved Manufacturers:** Vitro Certified™ Fabricator Required

**Certification:** Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation [Institute (www.c2ccertified.org](http://www.c2ccertified.org/)).

**Outdoor Appearance:** Ultra-neutral, light-gray

**Insulating Unit Construction:** 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Solar Control Low-E Insulating Glass

***“Solarban*®*”* 60 (2) *“Optiblue*®*”* + Clear (Formerly Solarban® z50)** by Vitro Architectural Glass

**Outdoor Lite: *“Solarban®* 60 (2) *Optiblue®”*** Glass by Vitro Architectural Glass, Sputter Coated on second surface (2)

**Indoor Lite:** Clear (transparent) Float Glass

**Low-E Coating: *“Solarban®”*** 60 Solar Control (Sputtered) by Vitro Architectural Glass

**Location:** Second Surface (2)

# Performance Values

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| 51% | 0.29 | 0.27 | 0.32 | 0.37 | 8% |

**Approved Manufacturers:** Vitro Certified™ Fabricator Required

**Certification:** Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation [Institute (www.c2ccertified.org](http://www.c2ccertified.org/)).

**Outdoor Appearance:** Steel blue-gray

**Insulating Unit Construction:** 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Solar Control Low-E Tinted Insulating Glass

***“Atlantica*®*”* + *“Solarban*®*”* 60 (3) Clear** by Vitro Architectural Glass

**Outdoor Lite: *“Atlantica®”*** Glass by Vitro Architectural Glass

**Indoor Lite:** Clear (transparent) Float Glass, Sputter Coated on third surface (3)

**Low-E Coating: *“Solarban®”*** 60 Solar Control (Sputtered) by Vitro Architectural Glass

**Location:** Third Surface (3)

# Performance Values

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| 53% | 0.29 | 0.27 | 0.27 | 0.32 | 9% |

**Approved Manufacturers:** Vitro Certified™ Fabricator Required

**Certification:** Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation [Institute (www.c2ccertified.org](http://www.c2ccertified.org/)).

**Outdoor Appearance:** Emerald-green

**Insulating Unit Construction:** 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Solar Control Low-E Tinted Insulating Glass

***“Azuria*®*”* + *“Solarban*®*”* 60 (3) Clear** by Vitro Architectural Glass

**Outdoor Lite: *“Azuria®”*** Glass by Vitro Architectural Glass

**Indoor Lite:** Clear (transparent) Float Glass, Sputter Coated on third surface (3)

**Low-E Coating: *“Solarban®”*** 60 Solar Control (Sputtered) by Vitro Architectural Glass

**Location:** Third Surface (3)

# Performance Values

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| 54% | 0.29 | 0.27 | 0.31 | 0.36 | 9% |

**Approved Manufacturers:** Vitro Certified™ Fabricator Required

**Certification:** Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation [Institute (www.c2ccertified.org](http://www.c2ccertified.org/)).

**Outdoor Appearance:** Aqua-blue

**Insulating Unit Construction:** 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Solar Control Low-E Tinted Insulating Glass

***“Graylite*®*”* II + *“Solarban*®*”* 60 (3) Clear** by Vitro Architectural Glass

**Outdoor Lite: *“Graylite®”*** II Glass by Vitro Architectural Glass

**Indoor Lite:** Clear (transparent) Float Glass, Sputter Coated on third surface (3)

**Low-E Coating: *“Solarban®”*** 60 Solar Control (Sputtered) by Vitro Architectural Glass

**Location:** Third Surface (3)

# Performance Values

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| 7% | 0.29 | 0.27 | 0.13 | 0.15 | 4% |

**Approved Manufacturers:** Vitro Certified™ Fabricator Required

**Certification:** Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation [Institute (www.c2ccertified.org](http://www.c2ccertified.org/)).

**Outdoor Appearance:** Dark-gray

**Insulating Unit Construction:** 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Solar Control Low-E Tinted Insulating Glass

***“Solarbronze*®” + *“Solarban*®*”* 60 (3) Clear** by Vitro Architectural Glass

**Outdoor Lite: “*Solarbronze®”*** Glass by Vitro Architectural Glass

**Indoor Lite:** Clear (transparent) Float Glass, Sputter Coated on third surface (3)

**Low-E Coating: *“Solarban®”*** 60 Solar Control (Sputtered) by Vitro Architectural Glass

**Location:** Third Surface (3)

# Performance Values

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| 42% | 0.29 | 0.27 | 0.32 | 0.37 | 7% |

**Approved Manufacturers:** Vitro Certified™ Fabricator Required

**Certification:** Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation [Institute (www.c2ccertified.org](http://www.c2ccertified.org/)).

**Outdoor Appearance:** Warm-bronze

**Insulating Unit Construction:** 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Solar Control Low-E Tinted Insulating Glass

***“Solargray*®*”* + *“Solarban*®*”* 60 (3) Clear** by Vitro Architectural Glass

**Outdoor Lite: “*Solargray®”*** Glass by Vitro Architectural Glass

**Indoor Lite:** Clear (transparent) Float Glass, Sputter Coated on third surface (3)

**Low-E Coating: *“Solarban®”*** 60 Solar Control (Sputtered) by Vitro Architectural Glass

**Location:** Third Surface (3)

# Performance Values

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| 35% | 0.29 | 0.27 | 0.29 | 0.33 | 7% |

**Approved Manufacturers:** Vitro Certified™ Fabricator Required

**Certification:** Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation [Institute (www.c2ccertified.org](http://www.c2ccertified.org/)).

**Outdoor Appearance:** Cool light-gray

**Insulating Unit Construction:** 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Solar Control Low-E Tinted Insulating Glass

***“Solexia*®*”* + *“Solarban*®*”* 60 (3) Clear** by Vitro Architectural Glass

**Outdoor Lite: *“Solexia®”*** Glass by Vitro Architectural Glass

**Indoor Lite:** Clear (transparent) Float Glass, Sputter Coated on third surface (3)

**Low-E Coating: *“Solarban®”*** 60 Solar Control (Sputtered) by Vitro Architectural Glass

**Location:** Third Surface (3)

# Performance Values

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| 61% | 0.29 | 0.27 | 0.37 | 0.42 | 10% |

**Approved Manufacturers:** Vitro Certified™ Fabricator Required

**Certification:** Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation [Institute (www.c2ccertified.org](http://www.c2ccertified.org/)).

**Outdoor Appearance:** Light-green

**Insulating Unit Construction:** 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Solar Control Low-E Tinted Insulating Glass

***“Solarblue*®” + *“Solarban*®” 60 (3) Clear** by Vitro Architectural Glass

**Outdoor Lite: *“Solarblue®”*** Glass by Vitro Architectural Glass

**Indoor Lite:** Clear (transparent) Float Glass, Sputter Coated on third surface (3)

**Low-E Coating: *“Solarban®”*** 60 Solar Control (Sputtered) by Vitro Architectural Glass

**Location:** Third Surface (3)

# Performance Values

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| 45% | 0.29 | 0.27 | 0.33 | 0.38 | 7% |

**Approved Manufacturers:** Vitro Certified™ Fabricator Required

**Certification:** Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation [Institute (www.c2ccertified.org](http://www.c2ccertified.org/)).

**Outdoor Appearance:** Light sky-blue

**Insulating Unit Construction:** 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Solar Control Low-E Tinted Insulating Glass

***“Pacifica*®*”* + *“Solarban*®*”* 60 (3) Clear** by Vitro Architectural Glass

**Outdoor Lite: *“Pacifica®”*** Glass by Vitro Architectural Glass

**Indoor Lite:** Clear (transparent) Float Glass, Sputter Coated on third surface (3)

**Low-E Coating: *“Solarban®”*** 60 Solar Control (Sputtered) by Vitro Architectural Glass

**Location:** Third Surface (3)

# Performance Values

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| 34% | 0.29 | 0.27 | 0.25 | 0.29 | 6% |

**Approved Manufacturers:** Vitro Certified™ Fabricator Required

**Certification:** Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation [Institute (www.c2ccertified.org](http://www.c2ccertified.org/)).

**Outdoor Appearance:** Deep-blue

**Insulating Unit Construction:** 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Solar Control Tinted Insulating Glass

***“Optigray*®*”* + *“Solarban*®*”* 60 (3) Clear** by Vitro Architectural Glass

**Outdoor Lite: “*Optigray®”*** Glass by Vitro Architectural Glass

**Indoor Lite:** Clear (transparent) Float Glass, Sputter Coated on third surface (3)

**Low-E Coating: *“Solarban®”*** 60 Solar Control (Sputtered) by Vitro Architectural Glass

**Location:** Third Surface (3)

# Performance Values

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| 50% | 0.29 | 0.27 | 0.35 | 0.40 | 8% |

**Approved Manufacturers:** Vitro Certified™ Fabricator Required

**Certification:** Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation [Institute (www.c2ccertified.org](http://www.c2ccertified.org/)).

**Outdoor Appearance:** Ultra-neutral, light-gray

**Insulating Unit Construction:** 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Subtly Reflective Tinted Solar Control Low-E Insulating Glass

***“Vistacool*®*”* (2) *“Azuria*®*”* + *“Solarban*®*”* 60 (3) Clear** by Vitro Architectural Glass

**Outdoor Lite: *“Azuria®”*** Glass by Vitro Architectural Glass

**Indoor Lite:** Clear (transparent) Float Glass, Sputter Coated on third surface (3)

**Low-E Coating: *“Solarban®”*** 60 Solar Control (Sputtered) by Vitro Architectural Glass **Location:** Third Surface (3)

**Reflective Coating: *“Vistacool®”*** by Vitro Architectural Glass

**Location:** Second Surface (2)

# Performance Values

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| 42% | 0.29 | 0.27 | 0.26 | 0.30 | 20% |

**Approved Manufacturers:** Vitro Certified™ Fabricator Required

**Certification:** Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation [Institute (www.c2ccertified.org](http://www.c2ccertified.org/)).

**Outdoor Appearance:** Subtly reflective aqua-blue

**Insulating Unit Construction:** 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Subtly Reflective Tinted Solar Control Low-E Insulating Glass

***“Vistacool*®*”* (2) *“Pacifica*®*”* + *“Solarban*®*”* 60 (3) Clear** by Vitro Architectural Glass

**Outdoor Lite: *“Pacifica®”*** Glass by Vitro Architectural Glass

**Indoor Lite:** Clear (transparent) Float Glass, Sputter Coated on third surface (3)

**Low-E Coating: *“Solarban®”*** 60 Solar Control (Sputtered), by Vitro Architectural Glass **Location:** Third Surface (3)

**Reflective Coating: *“Vistacool®”*** by Vitro Architectural Glass

**Location:** Second Surface (2)

# Performance Values

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| 26% | 0.29 | 0.27 | 0.22 | 0.25 | 11% |

**Approved Manufacturers:** Vitro Certified™ Fabricator Required

**Certification:** Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation [Institute (www.c2ccertified.org](http://www.c2ccertified.org/)).

**Outdoor Appearance:** Subtly reflective deep-blue

**Insulating Unit Construction:** 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Reflective Tinted Solar Control Low-E Insulating Glass

***“Solarcool*®*”* (2) *“Azuria*®*”* + *“Solarban*®*”* 60 (3) Clear** by Vitro Architectural Glass

**Outdoor Lite: *“Azuria®”*** Glass by Vitro Architectural Glass

**Indoor Lite:** Clear (transparent) Float Glass, Sputter Coated on third surface (3)

**Low-E Coating: *“Solarban®”*** 60 Solar Control (Sputtered) by Vitro Architectural Glass **Location:** Third Surface (3)

**Reflective Coating: *“Solarcool®”*** by Vitro Architectural Glass

**Location:** Second Surface (2)

# Performance Values

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| 21% | 0.29 | 0.27 | 0.17 | 0.19 | 19% |

**Approved Manufacturers:** Vitro Certified™ Fabricator Required

**Certification:** Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation [Institute (www.c2ccertified.org](http://www.c2ccertified.org/)).

**Outdoor Appearance:** Reflective aqua-blue

**Insulating Unit Construction:** 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Reflective Tinted Solar Control Low-E Insulating Glass

***“Solarcool*®*”* (2) “*Solarbronze*®” + *“Solarban*®*”* 60 (3) Clear** by Vitro Architectural Glass

**Outdoor Lite: “*Solarbronze®”*** Glass by Vitro Architectural Glass

**Indoor Lite:** Clear (transparent) Float Glass, Sputter Coated on third surface (3)

**Low-E Coating: *“Solarban®”*** 60 Solar Control (Sputtered) by Vitro Architectural Glass

**Location:** Third Surface (3)

**Reflective Coating: *“Solarcool®”*** by Vitro Architectural Glass

**Location:** Second Surface (2)

# Performance Values

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| 17% | 0.29 | 0.27 | 0.18 | 0.21 | 14% |

**Approved Manufacturers:** Vitro Certified™ Fabricator Required

**Certification:** Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation [Institute (www.c2ccertified.org](http://www.c2ccertified.org/)).

**Outdoor Appearance:** Reflective warm-bronze

**Insulating Unit Construction:** 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Reflective Tinted Solar Control Low-E Insulating Glass

***“Solarcool*®*”* (2) “*Solargray*®” + *“Solarban*®*”* 60 (3) Clear** by Vitro Architectural Glass

**Outdoor Lite: “*Solargray®”*** Glass by Vitro Architectural Glass

**Indoor Lite:** Clear (transparent) Float Glass, Sputter Coated on third surface (3)

**Low-E Coating: *“Solarban®”*** 60 Solar Control (Sputtered) by Vitro Architectural Glass

**Location:** Third Surface (3)

**Reflective Coating: *“Solarcool®”*** by Vitro Architectural Glass

**Location:** Second Surface (2)

# Performance Values

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| 14% | 0.29 | 0.27 | 0.17 | 0.20 | 11% |

**Approved Manufacturers:** Vitro Certified™ Fabricator Required

**Certification:** Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation [Institute (www.c2ccertified.org](http://www.c2ccertified.org/)).

**Outdoor Appearance:** Reflective cool light-gray

**Insulating Unit Construction:** 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Reflective Tinted Solar Control Low-E Insulating Glass

***“Solarcool*®*”* (2) *“Solarblue*®*”* + *“Solarban*®*”* 60 (3) Clear** by Vitro Architectural Glass

**Outdoor Lite: *“Solarblue®”*** Glass by Vitro Architectural Glass

**Indoor Lite:** Clear (transparent) Float Glass, Sputter Coated on third surface (3)

**Low-E Coating: *“Solarban®”*** 60 Solar Control (Sputtered) by Vitro Architectural Glass

**Location:** Third Surface (3)

**Reflective Coating: *“Solarcool®”*** by Vitro Architectural Glass

**Location:** Second Surface (2)

# Performance Values

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| 17% | 0.29 | 0.27 | 0.18 | 0.21 | 14% |

**Approved Manufacturers:** Vitro Certified™ Fabricator Required

**Certification:** Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation [Institute (www.c2ccertified.org](http://www.c2ccertified.org/)).

**Outdoor Appearance:** Reflective light sky-blue

**Insulating Unit Construction:** 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Reflective Tinted Solar Control Low-E Insulating Glass

***“Solarcool*®*”* (2) *“Pacifica*®*”* + *“Solarban*®*”* 60 (3) Clear** by Vitro Architectural Glass

**Outdoor Lite: *“Pacifica®”*** Glass by Vitro Architectural Glass

**Indoor Lite:** Clear (transparent) Float Glass, Sputter Coated on third surface (3)

**Low-E Coating: *“Solarban®”*** 60 Solar Control (Sputtered) by Vitro Architectural Glass **Location:** Third Surface (3)

**Reflective Coating: *“Solarcool®”*** by Vitro Architectural Glass

**Location:** Second Surface (2)

# Performance Values

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| 13% | 0.29 | 0.27 | 0.15 | 0.17 | 10% |

**Approved Manufacturers:** Vitro Certified™ Fabricator Required

**Certification:** Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation [Institute (www.c2ccertified.org](http://www.c2ccertified.org/)).

**Outdoor Appearance:** Reflective deep-blue

**Insulating Unit Construction:** 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass