# Type: Solar Control Low-E Clear Insulating Glass

“Solarban®” 72 (2) “Starphire®”  + “Starphire®” by Vitro Architectural Glass

Outdoor Lite: “Starphire®” Glass by Vitro Architectural Glass, Sputter Coated on second surface (2) for annealed and some heat-treated applications, depending on manufacturing process

Clear Glass by Vitro Architectural Glass, Sputter Coated on second surface (2) for heat-treated applications, depending on manufacturing process

Indoor Lite: “Starphire®” Glass by Vitro Architectural Glass

Low-E Coating: “Solarban®” 72 Solar Control (Sputtered) by Vitro Architectural Glass

Location: Second Surface (2)

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 68% | 0.28 | 0.26 | 0.28 | 0.32 | 13% |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

# Outdoor Appearance: Ultra-Clear

# Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Solar Control Low-E Clear Insulating Glass

“Solarban®” 72 (2) “Acuity™” + “Acuity™” by Vitro Architectural Glass

Outdoor Lite: “Acuity™” Glass by Vitro Architectural Glass, Sputter Coated on second surface (2) for annealed and some heat-treated applications, depending on manufacturing process

Clear Glass by Vitro Architectural Glass, Sputter Coated on second surface (2) for heat-treated applications, depending on manufacturing process

Indoor Lite: “Acuity™” Glass by Vitro Architectural Glass

Low-E Coating: “Solarban®” 72 Solar Control (Sputtered) by Vitro Architectural Glass

Location: Second Surface (2)

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 67% | 0.28 | 0.26 | 0.28 | 0.32 | 13% |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

# Outdoor Appearance: Ultra-Clear

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass