Type: Bird Safe Solar Control Low-E Clear Insulating Glass

“BirdSmart™ Speck 6 Inline 2x2 (1) Solarban® 65 (2) Clear + Clear” by Vitro Architectural Glass

Outdoor Lite: Clear Glass, “BirdSmart ™” Laser etch on first surface (1), Sputter Coated on second Surface (2) Float Glass by Vitro Architectural Glass

Indoor Lite: Clear (transparent) Float Glass

Laser Etch: “BirdSmart™ Speck Inline 2x2”, First Surface (1) by Vitro Architectural Glass

Low-E Coating: “Solarban® 65” Solar Control (Sputtered) by Vitro Architectural Glass

Location: Second Surface (2)

Performance Values

| Visible Light Transmittance | Exterior Light Reflectance | U-Value Winter Night | U-Value (Argon) | SHGC | CRI | Threat Factor |
| --- | --- | --- | --- | --- | --- | --- |
| 70% | 14% | 0.29 | 0.24 | 0.35 | 96 | 20 |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org). BirdSmart™ Speck 6 Inline 2x2 pattern threat factor certified by the American Bird Conservatory (ABC).

Outdoor Appearance: Clear

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

Type: Bird Safe Solar Control Low-E Ultra-Clear Insulating Glass

“BirdSmart™ Speck 6 Inline 2x2 (1) Solarban® 65 (2) Starphire® + Starphire®” by Vitro Architectural Glass

Outdoor Lite: Starphire® (low-iron) Glass, “BirdSmart ™” Laser-etch on first surface (1), Sputter Coated on second Surface (2) Float Glass by Vitro Architectural Glass

Indoor Lite: Starphire® (low-iron) Float Glass

Laser Etch: “BirdSmart™ Speck Inline 2x2”, First Surface (1) by Vitro Architectural Glass

Low-E Coating: “Solarban® 65” Solar Control (Sputtered) by Vitro Architectural Glass

Location: Second Surface (2)

Performance Values

| Visible Light Transmittance | Exterior Light Reflectance | U-Value Winter | U-Value (Argon) | SHGC | CRI | Threat Factor |
| --- | --- | --- | --- | --- | --- | --- |
| 73% | 15% | 0.29 | 0.24 | 0.36 | 99 | 20 |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org). BirdSmart™ Speck 6 Inline 2x2 pattern threat factor certified by the American Bird Conservatory (ABC).

Outdoor Appearance: Ultra-Clear

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

Type: Bird Safe Solar Control Low-E Ultra-Clear Glass Insulating Glass

“BirdSmart™ Speck 6 Inline 2x2 (1) Solarban® 65 (2) Acuity® + Acuity®” by Vitro Architectural Glass

Outdoor Lite: Acuity® (low-iron) Glass, “BirdSmart ™” Laser etch on first surface (1), Sputter Coated on second Surface (2) Float Glass by Vitro Architectural Glass

Indoor Lite: Acuity® (low-iron) Float Glass

Laser Etch: “BirdSmart™ Speck Inline 2x2”, First Surface (1) by Vitro Architectural Glass

Low-E Coating: “Solarban® 65” Solar Control (Sputtered) by Vitro Architectural Glass

Location: Second Surface (2)

Performance Values

| Visible Light Transmittance | Exterior Light Reflectance | U-Value Winter | U-Value (Argon) | SHGC | CRI | Threat Factor |
| --- | --- | --- | --- | --- | --- | --- |
| 72% | 15% | 0.29 | 0.24 | 0.36 | 98 | 20 |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org). BirdSmart™ Speck 6 Inline 2x2 pattern threat factor certified by the American Bird Conservatory (ABC).

Outdoor Appearance: Ultra-Clear

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

Type: Bird Safe Solar Control Low-E Clear Glass Insulating Glass

“BirdSmart™ Speck 6 Inline 2x4 (1) Solarban® 65 (2) Clear + Clear” by Vitro Architectural Glass

Outdoor Lite: Clear Glass, “BirdSmart ™” Laser etch on first surface (1), Sputter Coated on second Surface (2) Float Glass by Vitro Architectural Glass

Indoor Lite: Clear (transparent) Float Glass

Laser Etch: “BirdSmart™ Speck Inline 2x4”, First Surface (1) by Vitro Architectural Glass

Low-E Coating: “Solarban® 65” Solar Control (Sputtered) by Vitro Architectural Glass

Location: Second Surface (2)

Performance Values

| Visible Light Transmittance | Exterior Light Reflectance | U-Value Winter | U-Value (Argon) | SHGC | CRI | Threat Factor |
| --- | --- | --- | --- | --- | --- | --- |
| 70% | 14% | 0.29 | 0.24 | 0.35 | 96 | 25 |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org). BirdSmart™ Speck 6 Inline 2x4 pattern threat factor certified by the American Bird Conservatory (ABC).

Outdoor Appearance: Clear

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

Type: Bird Safe Solar Control Low-E Ultra-Clear Glass Insulating Glass

“BirdSmart™ Speck 6 Inline 2x4 (1) Solarban® 65 (2) Starphire® + Starphire®” by Vitro Architectural Glass

Outdoor Lite: Starphire® (low-iron) Glass, “BirdSmart ™” Laser-etch on first surface (1), Sputter Coated on second Surface (2) Float Glass by Vitro Architectural Glass

Indoor Lite: Starphire® (low-iron) Float Glass

Laser Etch: “BirdSmart™ Speck Inline 2x4”, First Surface (1) by Vitro Architectural Glass

Low-E Coating: “Solarban® 65” Solar Control (Sputtered) by Vitro Architectural Glass

Location: Second Surface (2)

Performance Values

| Visible Light Transmittance | Exterior Light Reflectance | U-Value Winter | U-Value (Argon) | SHGC | CRI | Threat Factor |
| --- | --- | --- | --- | --- | --- | --- |
| 73% | 15% | 0.29 | 0.24 | 0.36 | 99 | 25 |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org). BirdSmart™ Speck 6 Inline 2x4 pattern threat factor certified by the American Bird Conservatory (ABC).

Outdoor Appearance: Ultra-Clear

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

Type: Bird Safe Solar Control Low-E Ultra-Clear Glass Insulating Glass

“BirdSmart™ Speck 6 Inline 2x4 (1) Solarban® 65 (2) Acuity® + Acuity®” by Vitro Architectural Glass

Outdoor Lite: Acuity® (low-iron) Glass, “BirdSmart ™” Laser-etch on first surface (1), Sputter Coated on second Surface (2) Float Glass by Vitro Architectural Glass

Indoor Lite: Acuity® (low-iron) Float Glass

Laser Etch: “BirdSmart™ Speck Inline 2x4”, First Surface (1) by Vitro Architectural Glass

Low-E Coating: “Solarban® 65” Solar Control (Sputtered) by Vitro Architectural Glass

Location: Second Surface (2)

Performance Values

| Visible Light Transmittance | Exterior Light Reflectance | U-Value Winter | U-Value (Argon) | SHGC | CRI | Threat Factor |
| --- | --- | --- | --- | --- | --- | --- |
| 72% | 15% | 0.29 | 0.24 | 0.89 | 98 | 25 |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org). BirdSmart™ Speck 6 Inline 2x4 pattern threat factor certified by the American Bird Conservatory (ABC).

Outdoor Appearance: Ultra-Clear

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

Type: Bird Safe Solar Control Low-E Clear Glass Insulating Glass

“BirdSmart™ Speck 6 Shift 2x2 (1) Solarban® 65 (2) Clear + Clear” by Vitro Architectural Glass

Outdoor Lite: Clear Glass, “BirdSmart ™” Laser-etch on first surface (1), Sputter Coated on second Surface (2) Float Glass by Vitro Architectural Glass

Indoor Lite: Clear (transparent) Float Glass

Laser Etch: “BirdSmart™ Speck Shift 2x2”, First Surface (1) by Vitro Architectural Glass

Low-E Coating: “Solarban® 65” Solar Control (Sputtered) by Vitro Architectural Glass

Location: Second Surface (2)

Performance Values

| Visible Light Transmittance | Exterior Light Reflectance | U-Value Winter | U-Value (Argon) | SHGC | CRI | Threat Factor |
| --- | --- | --- | --- | --- | --- | --- |
| 70% | 14% | 0.29 | 0.24 | 0.35 | 96% | 20 |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org). BirdSmart™ Speck 6 Shift 2x2 pattern Threat factor certified by the American Bird Conservatory (ABC).

Outdoor Appearance: Clear

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

Type: Bird Safe Solar Control Low-E Ultra-Clear Glass Insulating Glass

“BirdSmart™ Speck 6 Shift 2x2 (1) Solarban® 65 (2) Starphire® + Starphire®” by Vitro Architectural Glass

Outdoor Lite: Starphire® (low-iron) Glass, “BirdSmart ™” Laser-etch on first surface (1), Sputter Coated on second Surface (2) Float Glass by Vitro Architectural Glass

Indoor Lite: Starphire® (low-iron) Float Glass

Laser Etch: “BirdSmart™ Speck Shift 2x2”, First Surface (1) by Vitro Architectural Glass

Low-E Coating: “Solarban® 65” Solar Control (Sputtered) by Vitro Architectural Glass

Location: Second Surface (2)

Performance Values

| Visible Light Transmittance | Exterior Light Reflectance | U-Value Winter | U-Value (Argon) | SHGC | CRI | Threat Factor |
| --- | --- | --- | --- | --- | --- | --- |
| 73% | 15% | 0.29 | 0.24 | 0.36 | 99 | 20 |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org). BirdSmart™ Speck 6 Shift 2x2 pattern Threat factor certified by the American Bird Conservatory (ABC).

Outdoor Appearance: Ultra-Clear

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

Type: Bird Safe Solar Control Low-E Ultra-Clear Glass Insulating Glass

“BirdSmart™ Speck 6 Shift 2x2 (1) Solarban® 65 (2) Acuity® + Acuity®” by Vitro Architectural Glass

Outdoor Lite: Acuity® (low-iron) Glass, “BirdSmart ™” Laser etch on first surface (1), Sputter Coated on second Surface (2) Float Glass by Vitro Architectural Glass

Indoor Lite: Acuity® (low-iron) Float Glass

Laser Etch: “BirdSmart™ Speck Shift 2x2”, First Surface (1) by Vitro Architectural Glass

Low-E Coating: “Solarban® 65” Solar Control (Sputtered) by Vitro Architectural Glass

Location: Second Surface (2)

Performance Values

| Visible Light Transmittance | Exterior Light Reflectance | U-Value Winter | U-Value (Argon) | SHGC | CRI | Threat Factor |
| --- | --- | --- | --- | --- | --- | --- |
| 72% | 15% | 0.29 | 0.24 | 0.36 | 98 | 20 |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org). BirdSmart™ Speck 6 Shift 2x2 pattern Threat factor certified by the American Bird Conservatory (ABC).

Outdoor Appearance: Ultra-Clear

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

Type: Bird Safe Solar Control Low-E Clear Glass Insulating Glass

“BirdSmart™ Speck 6 Shift 2x4 (1) Solarban® 65 (2) Clear + Clear” by Vitro Architectural Glass

Outdoor Lite: Clear Glass, “BirdSmart ™” Laser etch on first surface (1), Sputter Coated on second Surface (2) Float Glass by Vitro Architectural Glass

Indoor Lite: Clear (transparent) Float Glass

Laser Etch: “BirdSmart™ Speck Shift 2x4”, First Surface (1) by Vitro Architectural Glass

Low-E Coating: “Solarban® 65” Solar Control (Sputtered) by Vitro Architectural Glass

Location: Second Surface (2)

Performance Values

| Visible Light Transmittance | Exterior Light Reflectance | U-Value Winter | U-Value (Argon) | SHGC | CRI | Threat Factor |
| --- | --- | --- | --- | --- | --- | --- |
| 70% | 14% | 0.29 | 0.24 | 0.35 | 96 | 25 |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org). BirdSmart™ Speck 6 Shift 2x4 pattern Threat factor certified by the American Bird Conservatory (ABC).

Outdoor Appearance: Clear

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

Type: Bird Safe Solar Control Low-E Ultra-Clear Glass Insulating Glass

“BirdSmart™ Speck 6 Shift 2x4 (1) Solarban® 65 (2) Starphire® + Starphire®” by Vitro Architectural Glass

Outdoor Lite: Starphire® (low-iron) Glass, “BirdSmart ™” Laser etch on first surface (1), Sputter Coated on second Surface (2) Float Glass by Vitro Architectural Glass

Indoor Lite: Starphire® (low-iron) Float Glass

Laser Etch: “BirdSmart™ Speck Shift 2x4”, First Surface (1) by Vitro Architectural Glass

Low-E Coating: “Solarban® 65” Solar Control (Sputtered) by Vitro Architectural Glass

Location: Second Surface (2)

Performance Values

| Visible Light Transmittance | Exterior Light Reflectance | U-Value Winter | U-Value (Argon) | SHGC | CRI | Threat Factor |
| --- | --- | --- | --- | --- | --- | --- |
| 73% | 15% | 0.29 | 0.24 | 0.36 | 99 | 25 |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org). BirdSmart™ Speck 6 Shift 2x4 pattern Threat factor certified by the American Bird Conservatory (ABC).

Outdoor Appearance: Ultra-Clear

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

Type: Bird Safe Solar Control Low-E Ultra-Clear Glass Insulating Glass

“BirdSmart™ Speck 6 Shift 2x4 (1) Solarban® 65 (2) Acuity® + Acuity®” by Vitro Architectural Glass

Outdoor Lite: Acuity® (low-iron) Glass, “BirdSmart ™” Laser etch on first surface (1), Sputter Coated on second Surface (2) Float Glass by Vitro Architectural Glass

Indoor Lite: Acuity® (low-iron) Float Glass

Laser Etch: “BirdSmart™ Speck Shift 2x4”, First Surface (1) by Vitro Architectural Glass

Low-E Coating: “Solarban® 65” Solar Control (Sputtered) by Vitro Architectural Glass

Location: Second Surface (2)

Performance Values

| Visible Light Transmittance | Exterior Light Reflectance | U-Value Winter | U-Value (Argon) | SHGC | CRI | Threat Factor |
| --- | --- | --- | --- | --- | --- | --- |
| 72% | 15% | 0.29 | 0.24 | 0.36 | 98 | 25 |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org). BirdSmart™ Speck 6 Shift 2x4 pattern Threat factor certified by the American Bird Conservatory (ABC).

Outdoor Appearance: Ultra-Clear

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

Type: Bird Safe Solar Control Low-E Clear Glass Insulating Glass

“BirdSmart™ Speck 6 Inline 2x2 (1) Solarban® 70 (2)† + Clear” by Vitro Architectural Glass

Outdoor Lite: † Float Glass by Vitro Architectural Glass, “BirdSmart ™” Laser etch on first surface (1), Sputter Coated on second Surface (2)

Indoor Lite: Clear (transparent) Float Glass

Laser Etch: “BirdSmart™ Speck Inline 2x2”, First Surface (1) by Vitro Architectural Glass

Low-E Coating: “Solarban® 70” Solar Control (Sputtered) by Vitro Architectural Glass

Location: Second Surface (2)

†Solarban® 70 for annealed applications is applied to Acuity® glass; heat-treated applications will either require clear or Acuity® glass depending on manufacturing process.

Performance Values

| Visible Light Transmittance | Exterior Light Reflectance | U-Value Winter | U-Value (Argon) | SHGC | CRI | Threat Factor |
| --- | --- | --- | --- | --- | --- | --- |
| 64% | 13% | 0.28 | 0.24 | 0.27 | 91 | 20 |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Clear

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

Type: Bird Safe Solar Control Low-E Ultra-Clear Glass Insulating Glass

“BirdSmart™ Speck 6 Inline 2x2 (1) Solarban® 72 (2) Starphire® + Starphire®” by Vitro Architectural Glass

Outdoor Lite: Starphire® (low-iron) Glass, “BirdSmart ™” Laser etch on first surface (1), Sputter Coated on second Surface (2) Float Glass by Vitro Architectural Glass

Indoor Lite: Starphire® (low-iron) Float Glass

Laser Etch: “BirdSmart™ Speck Inline 2x2”, First Surface (1) by Vitro Architectural Glass

Low-E Coating: “Solarban® 72” Solar Control (Sputtered) by Vitro Architectural Glass

Location: Second Surface (2)

Performance Values

| Visible Light Transmittance | Exterior Light Reflectance | U-Value Winter | U-Value (Argon) | SHGC | CRI | Threat Factor |
| --- | --- | --- | --- | --- | --- | --- |
| 68% | 13% | 0.28 | 0.24 | 0.28 | 95 | 20 |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org). BirdSmart™ Speck 6 Inline 2x2 pattern Threat factor certified by the American Bird Conservatory (ABC).

Outdoor Appearance: Ultra-Clear

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

Type: Bird Safe Solar Control Low-E Ultra-Clear Glass Insulating Glass

“BirdSmart™ Speck 6 Inline 2x2 (1) Solarban® 72 (2) Acuity® + Acuity®” by Vitro Architectural Glass

Outdoor Lite: Acuity® (low-iron) Glass, “BirdSmart ™” Laser etch on first surface (1), Sputter Coated on second Surface (2) Float Glass by Vitro Architectural Glass

Indoor Lite: Acuity® (low-iron) Float Glass

Laser Etch: “BirdSmart™ Speck Inline 2x2”, First Surface (1) by Vitro Architectural Glass

Low-E Coating: “Solarban® 72” Solar Control (Sputtered) by Vitro Architectural Glass

Location: Second Surface (2)

Performance Values

| Visible Light Transmittance | Exterior Light Reflectance | U-Value Winter | U-Value (Argon) | SHGC | CRI | Threat Factor |
| --- | --- | --- | --- | --- | --- | --- |
| 67% | 13% | 0.28 | 0.24 | 0.28 | 94 | 20 |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org). BirdSmart™ Speck 6 Inline 2x2 pattern threat factor certified by the American Bird Conservatory (ABC).

Outdoor Appearance: Ultra-Clear

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

Type: Bird Safe Solar Control Low-E Clear Glass Insulating Glass

“BirdSmart™ Speck 6 Inline 2x4 (1) Solarban® 70 (2) † + Clear” by Vitro Architectural Glass

Outdoor Lite: † Float Glass by Vitro Architectural Glass, “BirdSmart ™” Laser etch on first surface (1), Sputter Coated on second Surface (2)

Indoor Lite: Clear (transparent) Float Glass

Laser Etch: “BirdSmart™ Speck Inline 2x4”, First Surface (1) by Vitro Architectural Glass

Low-E Coating: “Solarban® 70” Solar Control (Sputtered) by Vitro Architectural Glass

Location: Second Surface (2)

†Solarban® 70 for annealed applications is applied to Acuity® glass; heat-treated applications will either require clear or Acuity® glass depending on manufacturing process.

Performance Values

| Visible Light Transmittance | Exterior Light Reflectance | U-Value Winter | U-Value (Argon) | SHGC | CRI | Threat Factor |
| --- | --- | --- | --- | --- | --- | --- |
| 64% | 13% | 0.28 | 0.24 | 0.27 | 91 | 25 |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org). BirdSmart™ Speck 6 Inline 2x4 pattern threat factor certified by the American Bird Conservatory (ABC).

Outdoor Appearance: Clear

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

Type: Bird Safe Solar Control Low-E Ultra-Clear Glass Insulating Glass

“BirdSmart™ Speck 6 Inline 2x4 (1) Solarban® 72 (2) Starphire® + Starphire®” by Vitro Architectural Glass

Outdoor Lite: Starphire® (low-iron) Glass, “BirdSmart ™” Laser etch on first surface (1), Sputter Coated on second Surface (2) Float Glass by Vitro Architectural Glass

Indoor Lite: Starphire® (low-iron) Float Glass

Laser Etch: “BirdSmart™ Speck Inline 2x4”, First Surface (1) by Vitro Architectural Glass

Low-E Coating: “Solarban® 72” Solar Control (Sputtered) by Vitro Architectural Glass

Location: Second Surface (2)

Performance Values

| Visible Light Transmittance | Exterior Light Reflectance | U-Value Winter | U-Value (Argon) | SHGC | CRI | Threat Factor |
| --- | --- | --- | --- | --- | --- | --- |
| 68% | 13% | 0.28 | 0.24 | 0.28 | 95 | 25 |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org). BirdSmart™ Speck 6 Inline 2x4 pattern threat factor certified by the American Bird Conservatory (ABC).

Outdoor Appearance: Ultra-Clear

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

Type: Bird Safe Solar Control Low-E Ultra-Clear Glass Insulating Glass

“BirdSmart™ Speck 6 Inline 2x4 (1) Solarban® 72 (2) Acuity® + Acuity®” by Vitro Architectural Glass

Outdoor Lite: Acuity® (low-iron) Glass, “BirdSmart ™” Laser etch on first surface (1), Sputter Coated on second Surface (2) Float Glass by Vitro Architectural Glass

Indoor Lite: Acuity® (low-iron) Float Glass

Laser Etch: “BirdSmart™ Speck Inline 2x4”, First Surface (1) by Vitro Architectural Glass

Low-E Coating: “Solarban® 72” Solar Control (Sputtered) by Vitro Architectural Glass

Location: Second Surface (2)

Performance Values

| Visible Light Transmittance | Exterior Light Reflectance | U-Value Winter | U-Value (Argon) | SHGC | CRI | Threat Factor |
| --- | --- | --- | --- | --- | --- | --- |
| 67% | 13% | 0.28 | 0.24 | 0.28 | 94 | 25 |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org). BirdSmart™ Speck 6 Inline 2x4 pattern threat factor certified by the American Bird Conservatory (ABC).

Outdoor Appearance: Ultra-Clear

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

Type: Bird Safe Solar Control Low-E Clear Glass Insulating Glass

“BirdSmart™ Speck 6 Shift 2x2 (1) Solarban® 70 (2)† + Clear” by Vitro Architectural Glass

Outdoor Lite: † Float Glass by Vitro Architectural Glass, “BirdSmart ™” Laser etch on first surface (1), Sputter Coated on second Surface (2)

Indoor Lite: Clear (transparent) Float Glass

Laser Etch: “BirdSmart™ Speck Shift 2x2”, First Surface (1) by Vitro Architectural Glass

Low-E Coating: “Solarban® 70” Solar Control (Sputtered) by Vitro Architectural Glass

Location: Second Surface (2)

†Solarban® 70 for annealed applications is applied to Acuity® glass; heat-treated applications will either require clear or Acuity® glass depending on manufacturing process.

Performance Values

| Visible Light Transmittance | Exterior Light Reflectance | U-Value Winter | U-Value (Argon) | SHGC | CRI | Threat Factor |
| --- | --- | --- | --- | --- | --- | --- |
| 64% | 13% | 0.28 | 0.24 | 0.27 | 91 | 20 |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org). BirdSmart™ Speck 6 Shift 2x2 pattern threat factor certified by the American Bird Conservatory (ABC).

Outdoor Appearance: Clear

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

Type: Bird Safe Solar Control Low-E Ultra-Clear Glass Insulating Glass

“BirdSmart™ Speck 6 Shift 2x2 (1) Solarban® 72 (2) Starphire® + Starphire®” by Vitro Architectural Glass

Outdoor Lite: Starphire® (low-iron) Glass, “BirdSmart ™” Laser etch on first surface (1), Sputter Coated on second Surface (2) Float Glass by Vitro Architectural Glass

Indoor Lite: Starphire® (low-iron) Float Glass

Laser Etch: “BirdSmart™ Speck Shift 2x2”, First Surface (1) by Vitro Architectural Glass

Low-E Coating: “Solarban® 72” Solar Control (Sputtered) by Vitro Architectural Glass

Location: Second Surface (2)

Performance Values

| Visible Light Transmittance | Exterior Light Reflectance | U-Value Winter | U-Value (Argon) | SHGC | CRI | Threat Factor |
| --- | --- | --- | --- | --- | --- | --- |
| 68% | 13% | 0.28 | 0.24 | 0.28 | 95 | 20 |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org). BirdSmart™ Speck 6 Shift 2x2 pattern threat factor certified by the American Bird Conservatory (ABC).

Outdoor Appearance: Ultra-Clear

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

Type: Bird Safe Solar Control Low-E Ultra-Clear Glass Insulating Glass

“BirdSmart™ Speck 6 Shift 2x2 (1) Solarban® 72 (2) Acuity® + Acuity®” by Vitro Architectural Glass

Outdoor Lite: Acuity® (low-iron) Glass, “BirdSmart ™” Laser etch on first surface (1), Sputter Coated on second Surface (2) Float Glass by Vitro Architectural Glass

Indoor Lite: Acuity® (low-iron) Float Glass

Laser Etch: “BirdSmart™ Speck Shift 2x2”, First Surface (1) by Vitro Architectural Glass

Low-E Coating: “Solarban® 72” Solar Control (Sputtered) by Vitro Architectural Glass

Location: Second Surface (2)

Performance Values

| Visible Light Transmittance | Exterior Light Reflectance | U-Value Winter | U-Value (Argon) | SHGC | CRI | Threat Factor |
| --- | --- | --- | --- | --- | --- | --- |
| 67% | 13% | 0.28 | 0.24 | 0.28 | 94 | 20 |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org). BirdSmart™ Speck 6 Shift 2x2 pattern threat factor certified by the American Bird Conservatory (ABC).

Outdoor Appearance: Ultra-Clear

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

Type: Bird Safe Solar Control Low-E Clear Glass Insulating Glass

“BirdSmart™ Speck 6 Shift 2x4 (1) Solarban® 70 (2)† + Clear” by Vitro Architectural Glass

Outdoor Lite: † Float Glass by Vitro Architectural Glass, “BirdSmart ™” Laser etch on first surface (1), Sputter Coated on second Surface (2)

Indoor Lite: Clear (transparent) Float Glass

Laser Etch: “BirdSmart™ Speck Shift 2x4”, First Surface (1) by Vitro Architectural Glass

Low-E Coating: “Solarban® 70” Solar Control (Sputtered) by Vitro Architectural Glass

Location: Second Surface (2)

†Solarban® 70 for annealed applications is applied to Acuity® glass; heat-treated applications will either require clear or Acuity® glass depending on manufacturing process.

Performance Values

| Visible Light Transmittance | Exterior Light Reflectance | U-Value Winter | U-Value (Argon) | SHGC | CRI | Threat Factor |
| --- | --- | --- | --- | --- | --- | --- |
| 64% | 13% | 0.28 | 0.24 | 0.27 | 91 | 25 |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org). BirdSmart™ Speck 6 Shift 2x4 pattern threat factor certified by the American Bird Conservatory (ABC).

Outdoor Appearance: Clear

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

Type: Bird Safe Solar Control Low-E Ultra-Clear Glass Insulating Glass

“BirdSmart™ Speck 6 Shift 2x4 (1) Solarban® 72 (2) Starphire® + Starphire®” by Vitro Architectural Glass

Outdoor Lite: Starphire® (low-iron) Glass, “BirdSmart ™” Laser etch on first surface (1), Sputter Coated on second Surface (2) Float Glass by Vitro Architectural Glass

Indoor Lite: Starphire® (low-iron) Float Glass

Laser Etch: “BirdSmart™ Speck Shift 2x4”, First Surface (1) by Vitro Architectural Glass

Low-E Coating: “Solarban® 72” Solar Control (Sputtered) by Vitro Architectural Glass

Location: Second Surface (2)

Performance Values

| Visible Light Transmittance | Exterior Light Reflectance | U-Value Winter | U-Value (Argon) | SHGC | CRI | Threat Factor |
| --- | --- | --- | --- | --- | --- | --- |
| 68% | 13% | 0.28 | 0.24 | 0.28 | 95 | 25 |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org). BirdSmart™ Speck 6 Shift 2x4 pattern threat factor certified by the American Bird Conservatory (ABC).

Outdoor Appearance: Ultra-Clear

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

Type: Bird Safe Solar Control Low-E Ultra-Clear Glass Insulating Glass

“BirdSmart™ Speck 6 Shift 2x4 (1) Solarban® 72 (2) Acuity® + Acuity®” by Vitro Architectural Glass

Outdoor Lite: Acuity® (low-iron) Glass, “BirdSmart ™” Laser etch on first surface (1), Sputter Coated on second Surface (2) Float Glass by Vitro Architectural Glass

Indoor Lite: Acuity® (low-iron) Float Glass

Laser Etch: “BirdSmart™ Speck Shift 2x4”, First Surface (1) by Vitro Architectural Glass

Low-E Coating: “Solarban® 72” Solar Control (Sputtered) by Vitro Architectural Glass

Location: Second Surface (2)

Performance Values

| Visible Light Transmittance | Exterior Light Reflectance | U-Value Winter | U-Value (Argon) | SHGC | CRI | Threat Factor |
| --- | --- | --- | --- | --- | --- | --- |
| 67% | 13% | 0.28 | 0.24 | 0.28 | 94 | 25 |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org). BirdSmart™ Speck 6 Shift 2x4 pattern threat factor certified by the American Bird Conservatory (ABC).

Outdoor Appearance: Ultra-Clear

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass