# Type: Solar Control Low-iron Low-E Clear Insulating Glass

“Solarban®” 60 (2) “Starphire®” + “Starphire®” by Vitro Architectural Glass

Outdoor Lite: “Starphire®” (low-iron) Float Glass by Vitro Architectural Glass, Sputter Coated on second surface (2)

Indoor Lite: “Starphire®” (low-iron) Float Glass

Low-E Coating: “Solarban®” 60 Solar Control (Sputtered) by Vitro Architectural Glass

Location: Second Surface (2)

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 74% | 0.29 | 0.27 | 0.41 | 0.48 | 11% |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Low-iron

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Solar Control Low-iron Low-E Insulating Glass

“Solarban®” 90 (2) “Starphire®” + “Starphire®” by Vitro Architectural Glass

Outdoor Lite: “Starphire®” Glass by Vitro Architectural Glass, Sputter Coated on second surface (2)

Indoor Lite: “Starphire®” Glass

Low-E Coating: “Solarban®” 90 Solar Control (Sputtered) by Vitro Architectural Glass

Location: Second Surface (2)

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 54% | 0.29 | 0.27 | 0.23 | 0.26 | 13% |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

# Outdoor Appearance: Clear

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Uncoated Low-iron Float Glass

“Starphire®” + “Starphire®” by Vitro Architectural Glass

Outdoor Lite: “Starphire®” (low-iron) Float Glass by Vitro Architectural Glass

Indoor Lite: “Starphire®” (low-iron) Float Glass by Vitro Architectural Glass

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 84% | 0.47 | 0.50 | 0.82 | 0.94 | 15% |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Low-iron

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Solar Control Low-iron Low-E Clear Insulating Glass

“Solarban®” 60 (2) “Acuity™” + “Acuity™” by Vitro Architectural Glass

Outdoor Lite: “Acuity™” (low-iron) Float Glass by Vitro Architectural Glass, Sputter Coated on second surface (2)

Indoor Lite: “Acuity™” (low-iron) Float Glass

Low-E Coating: “Solarban®” 60 Solar Control (Sputtered) by Vitro Architectural Glass

Location: Second Surface (2)

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 73% | 0.29 | 0.27 | 0.41 | 0.47 | 11% |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Low-iron

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Solar Control Low-iron Low-E Insulating Glass

“Solarban®” 90 (2) “Acuity™” + “Acuity™” by Vitro Architectural Glass

Outdoor Lite: “Acuity™” Glass by Vitro Architectural Glass, Sputter Coated on second surface (2)

Indoor Lite: “Acuity™” Glass

Low-E Coating: “Solarban®” 90 Solar Control (Sputtered) by Vitro Architectural Glass

Location: Second Surface (2)

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 53% | 0.29 | 0.27 | 0.23 | 0.27 | 12% |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

# Outdoor Appearance: Clear

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Uncoated Low-iron Float Glass

“Acuity™” + “Acuity™” by Vitro Architectural Glass

Outdoor Lite: “Acuity™” (low-iron) Float Glass by Vitro Architectural Glass

Indoor Lite: “Acuity™” (low-iron) Float Glass by Vitro Architectural Glass

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 82% | 0.47 | 0.50 | 0.78 | 0.90 | 15% |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Low-iron

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass