# Type: Low-E Clear Insulating Glass

“Sungate®” 400 (2) Clear + Clear by Vitro Architectural Glass

Outdoor Lite: Clear (transparent) Float Glass, Sputter Coated on second surface (2)

Indoor Lite: Clear (transparent) Float Glass

Low-E Coating: “Sungate®” 400 (Sputtered) by Vitro Architectural Glass

Location: Second Surface (2)

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 76% | 0.32 | 0.31 | 0.60 | 0.69 | 14% |

Approved Manufacturers: Vitro-specific approval not required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

# Outdoor Appearance: Clear

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Low-E Tinted Insulating Glass

Clear + “Sungate®” 400 (3) Clear by Vitro Architectural Glass

Outdoor Lite: Clear (transparent) Float Glass

Indoor Lite: Clear (transparent) Float Glass, Sputter Coated on third surface (3) Low-E Coating: “Sungate®” 400 (Sputtered) by Vitro Architectural Glass Location: Third Surface (3)

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 76% | 0.32 | 0.31 | 0.63 | 0.73 | 14% |

Approved Manufacturers: Vitro-specific approval not required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

# Outdoor Appearance: Clear

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Low-E Clear Insulating Glass

“Sungate®” 400 (2) “Starphire®” + “Starphire®”  by Vitro Architectural Glass

Outdoor Lite: “Starphire®” (low-iron [a specially formulated glass type to eliminate the green hue commonly associated with clear glass]) Float Glass by Vitro Architectural Glass, Sputter Coated on second surface (2)

Indoor Lite: “Starphire®” (low-iron) Float Glass

Low-E Coating: “Sungate®” 400 (Sputtered) by Vitro Architectural Glass

Location: Second Surface (2)

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 80% | 0.32 | 0.31 | 0.68 | 0.78 | 14% |

Approved Manufacturers: Vitro-specific approval not required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

# Outdoor Appearance: Clear

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Low-E Tinted Insulating Glass

“Solexia®” + “Sungate®” 400 (3) Clear by Vitro Architectural Glass

Outdoor Lite: “Solexia®” Glass by Vitro Architectural Glass

Indoor Lite: Clear (transparent) Float Glass, Sputter Coated on third surface (3) Low-E Coating: “Sungate®” 400 (Sputtered) by Vitro Architectural Glass Location: Third Surface (3)

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 66% | 0.32 | 0.31 | 0.44 | 0.50 | 11% |

Approved Manufacturers: Vitro-specific approval not required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Light-green

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Low-E Tinted Insulating Glass

“Atlantica®” + “Sungate®” 400 (3) Clear by Vitro Architectural Glass

Outdoor Lite: “Atlantica®” Glass by Vitro Architectural Glass

Indoor Lite: Clear (transparent) Float Glass, Sputter Coated on third surface (3) Low-E Coating: “Sungate®” 400 (Sputtered) by Vitro Architectural Glass Location: Third Surface (3)

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 58% | 0.32 | 0.31 | 0.35 | 0.40 | 9% |

Approved Manufacturers: Vitro-specific approval not required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Emerald-green

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Low-E Tinted Insulating Glass

“Azuria®” + “Sungate®” 400 (3) Clear by Vitro Architectural Glass

Outdoor Lite: “Azuria®” Glass by Vitro Architectural Glass

Indoor Lite: Clear (transparent) Float Glass Sputter Coated on third surface (3) Low-E Coating: “Sungate®” 400 (Sputtered) by Vitro Architectural Glass Location: Third Surface (3)

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 59% | 0.32 | 0.31 | 0.34 | 0.39 | 10% |

Approved Manufacturers: Vitro-specific approval not required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Aqua-blue

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Low-E Tinted Insulating Glass

“Solarbronze®” + “Sungate®” 400 (3) Clear by Vitro Architectural Glass

Outdoor Lite: “Solarbronze®” Glass by Vitro Architectural Glass

Indoor Lite: Clear (transparent) Float Glass Sputter Coated on third surface (3) Low-E Coating: “Sungate®” 400 (Sputtered) by Vitro Architectural Glass Location: Third Surface (3)

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 46% | 0.32 | 0.31 | 0.44 | 0.50 | 8% |

Approved Manufacturers: Vitro-specific approval not required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Warm-bronze

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Low-E Tinted Insulating Glass

“Solargray®” + “Sungate®” 400 (3) Clear by Vitro Architectural Glass

Outdoor Lite: “Solargray®” Glass by Vitro Architectural Glass

Indoor Lite: Clear (transparent) Float Glass Sputter Coated on third surface (3) Low-E Coating: “Sungate®” 400 (Sputtered) by Vitro Architectural Glass Location: Third Surface (3)

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 38% | 0.32 | 0.31 | 0.39 | 0.44 | 7% |

Approved Manufacturers: Vitro-specific approval not required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Cool light-gray

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Reflective Tinted Low-E Insulating Glass

“Graylite®” II + “Sungate®” 400 (3) Clear by Vitro Architectural Glass

Outdoor Lite: “Graylite®” II Glass by Vitro Architectural Glass

Indoor Lite: Clear (transparent) Float Glass Sputter Coated on third surface (3) Low-E Coating: “Sungate®” 400 (Sputtered) by Vitro Architectural Glass Location: Third Surface (3)

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 8% | 0.32 | 0.31 | 0.15 | 0.17 | 4% |

Approved Manufacturers: Vitro-specific approval not required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Dark-gray

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Low-E Tinted Insulating Glass

“Solarblue®” + “Sungate®” 400 (3) Clear by Vitro Architectural Glass

Outdoor Lite: “Solarblue®” Glass by Vitro Architectural Glass

Indoor Lite: Clear (transparent) Float Glass Sputter Coated on third surface (3) Low-E Coating: “Sungate®” 400 (Sputtered) by Vitro Architectural Glass Location: Third Surface (3)

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 48% | 0.32 | 0.31 | 0.42 | 0.49 | 8% |

Approved Manufacturers: Vitro-specific approval not required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Light sky-blue

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Low-E Tinted Insulating Glass

“Pacifica®” +“Sungate®” 400 (3) Clear by Vitro Architectural Glass

Outdoor Lite: “Pacifica®” Glass by Vitro Architectural Glass

Indoor Lite: Clear (transparent) Float Glass Sputter Coated on third surface (3) Low-E Coating: “Sungate®” 400 (Sputtered) by Vitro Architectural Glass Location: Third Surface (3)

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 37% | 0.32 | 0.31 | 0.30 | 0.34 | 7% |

Approved Manufacturers: Vitro-specific approval not required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Deep-blue

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Low-E Tinted Insulating Glass

“Optigray®” + “Sungate®” 400 (3) Clear by Vitro Architectural Glass

Outdoor Lite: “Optigray®” Glass by Vitro Architectural Glass

Indoor Lite: Clear (transparent) Float Glass Sputter Coated on third surface (3) Low-E Coating: “Sungate®” 400 (Sputtered) by Vitro Architectural Glass Location: Third Surface (3)

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 54% | 0.32 | 0.31 | 0.46 | 0.52 | 9% |

Approved Manufacturers: Vitro-specific approval not required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Ultra-neutral, light-gray

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass